# INTRODUCTION

This document will be updated with the notes made during class.  The document will be made available in MS WORD format to allow students access to the Excel spreadsheets that were included during class.  Please note that this document was compiled during class and was not proof read for typing, language, and calculation errors.  Please inform the lecturer should you detect any serious errors.

# MOHR DIAGRAM AND DIRECTION OF STRESS

σ

τ

τa

σ1

# GOODMAN MEAN STRESS CORRECTION

We calculate the equivalent completely reversed stress amplitude that represent the non-zero mean stress that was applied and can be used on the S-N curve.

σaσar+σmσu=1
σar=σa1-σmσu

# STRESS-LIFE EXAMPLE DONE IN CLASS

## Problem statement

## Solution

Methodology:

- Calculate my endurance limit, including modification factors, to see if there are any completely stress amplitudes that exceeds the endurance limit.

  - Goodman mean stress correction.

  - Calculate the modifying factors.

  - Calculate the fatigue notch factor.

σer=σerb'CsizeCloadCsurfCTCrel
σerb'=0.5σuKf

- If the stress spectrum contains completely reversed stress amplitudes that exceed the endurance limit, construct the S-N curve.

σar,103=σarb,103'CloadCTCrel
σarb,103'=0.9σuKf'

- Use Palmgren-Miner rule and calculate total damage.

- Calculate number of repetitions and fatigue life.

### Fatigue notch factor at 1 million cycles, Kf

The theoretical stress concentration factor was given as Kt=2.

Kf=1+Kt-11+αr

- Approximations for α:

α=300σuksi1.8×10-3 in.
=300×6.8910501.8×10-3×25.4 mm
=0.086 mm

From this, we have:

Kf=1+Kt-11+αr
=1+2-11+0.0864
=1.98

### Fatigue notch factor at 1 000 cycles, Kf'

The ultimate tensile strength is 1050 MPa (=152 ksi).  The notch sensitivity factor at 1 000 cycles is then q=0.36, from which:

Kf'-1Kf-1=q=0.36
Kf'=0.361.98-1+1
=1.35

### Modification factor: Size, Csize

σer=σerb'CsizeCloadCsurfCTCrel
σerb'=0.5σuKf

Csize=1.0, if d≤8 mm1.189d-0.097,if 8 mm<d≤250 mm

In this case, the diameter is 200 mm.

Csiz=1.189×200-0.097
=0.71

### Modification factor: Load, Cload

The component will be subject to cyclic axial stress.  The S-N curve that we will construct, will be from a rotating bending test.  So, we have to do modification for load because of the larger volume that the axially loaded specimen will be subject to.

Cload=0.70

### Modification factor: Surface finish, Csurf

It is assumed that the machined surface is corrosion protected.  Therefore, the modification factor for surface finish is Csurf=0.70:

### Modification factor: Temperature, CT

The component is subject to an operating temperature T=500 ℃.  From this, the modification factor for temperature is:

CT=1.0 for T≤450 ℃1-5.8-3T-450, for 450<T≤550 ℃
=1-5.8-3500-450
=0.74

### Modification factor: Reliability, Crel

For a 1% probability of failure, we have a 99% probability of survival, and Crel=0.814.

### Endurance limit after modification

The endurance limit after applying modification factors is 55.6 MPa, which is clearly below the stress amplitudes applied to the specimen (shown in the table below) and we need to construct the fatigue curve because we will have finite life in this case.

σerb'=0.5σuKf
σer=σerb'CsizeCloadCsurfCTCrel
=0.5×10501.98∙0.71∙0.70∙0.70∙0.74∙0.814
=55.6 MPa

### Construct the S-N curve

The fatigue strength at 1 000 cycles is:

σarb,103'=0.9σuKf'
σar,103=σarb,103'CloadCTCrel
=0.9∙10501.35∙0.7∙0.74∙0.814
=295.2 MPa

For the part of the S-N curve below 295.2 MPa and above 55.6 MPa, the following applies:

S1mN1=S2mN2
mlog10S1S2=log10N2N1
m=log10N2N1log10S1S2
=log101000log10296.255.6
=4.13

### Goodman mean stress modification

σar=σa1-σmσu

### Damage and life

For σa,σm=[100, 200] applied for n=10 000 cycles we have:

- Goodman completely reversed stress amplitude is:

σar=σa1-σmσu
=1001-2001050
=123.5 MPa

- The endurance is then:

NR=σar,1σarmN10.9σu≥σar≥σer∞σar<σer
=55.6σar4.131060.9σu≥σar≥σer∞σar<σer
=55.6123.54.13106
=35 818

- Damage:

d1=10 00035 818
=0.28

### Damage and life

For σa,σm=[50, 0] applied for n=5 000 cycles we have:

- Goodman completely reversed stress amplitude is:

σar=σa1-σmσu
=501-01050
=50 MPa

- The endurance is then:

NR=σar,1σarmN10.9σu≥σar≥σer∞σar<σer
=55.6σar4.131060.9σu≥σar≥σer∞σar<σer
=∞

- Damage:

d2=5 000∞
=0

For σa,σm=[100, 100] applied for n=20 000 cycles we have:

- Goodman completely reversed stress amplitude is:

σar=σa1-σmσu
=1001-1001050
=110.5 MPa

- The endurance is then:

NR=σar,1σarmN10.9σu≥σar≥σer∞σar<σer
=55.6σar4.131060.9σu≥σar≥σer∞σar<σer
=55.6110.54.13106
=58 623 cycles

- Damage:

d3=20 00058 623
=0.34

For σa,σm=[200, -100] applied for n=2 000 cycles we have:

- Goodman completely reversed stress amplitude is:

σar=σa1-σmσu
=2001--1001050
=182.6 MPa

- The endurance is then:

NR=σar,1σarmN10.9σu≥σar≥σer∞σar<σer
=55.6σar4.131060.9σu≥σar≥σer∞σar<σer
=55.6182.64.13106
=7 364 cycles

- Damage:

d4=2 0007 364
=0.27

The total damage is then:

D=d1+d2+d3+d4
=0.28+0+0.34+0.27
=0.89

The number of repetitions of the 3-month stress spectrum is:

Bf=1D
=1.12

The fatigue life for this component for a 1% probability of failure is:

L=Period of stress spectrum×Bf
=Period of stress spectrumD
=3×1.12
=3.36 months

# PROBLEM 2019-08-14: STRESS LIFE CLASS PROBLEM

## Problem statement

Component undergoes axial cyclic stress as follows:

| Stress amplitude [MPa] | Stress mean [MPa] | Number of cycles/block |
| --- | --- | --- |
| 100 | 200 | 10000 |
| 50 | 0 | 5000 |
| 100 | 100 | 20000 |
| 200 | -100 | 2000 |

Material is steel with Sut = 1,050MPa with hardness 350 BHN.  The theoretical stress concentration factor at a notch on the part is Kt=2.  The notch radius is r=4 mm.  The surface finish is machined.  The shaft has a radius of 100 mm and operates at temperature T=200 °C

How many blocks of loading can be loaded on the component for a 1 % probability of fatigue crack initiation?  That is, what is the fatigue life of the component?

## Solution

Step 1:  Construct the S-N curve for the material

We need the following:

S103=0.9fuKf'CloadCrelCT, at N=103cycles

Se=0.5fuKfCloadCrelCTCsizeCsurf, at N=106

Step 2:  Calculate the influencing factors

Fatigue notch factor

The fatigue notch factor at endurance, Kf, is as follows:

Kf=1+Kt-11+ar
a=300σuksi1.8×10-3 in.
=30010506.891.8×10-3×25.4 mm
=0.0859 mm
Kf=1.98

The notch fatigue factor at 1 000 cycles, Kf', is then:

Kf'-1Kf-1=fσu=q

From the figure below at ultimate tensile strength 1 0506.89~150 ksi, the fatigue notch sensitivity factor (from the figure below) is:

q=0.4

From this:

Kf'-1Kf-1=q
Kf'=qKf-1+1
=1.39

Modification factor: Load

For axial loading, the load factor is:

Cload=0.7

Modification factor: Reliability

The client requested a 1% probability of crack initiation, which is a 99% probability6 of survival.

From the table below, the modification factor for reliability is:

Crel=0.814

Modification factor: Temperature

The operating temperature was given as T=200 °C.  Therefore, the modification factor is:

CT=1.0 for T≤450 ℃1-5.8-3T-450, for 450<T≤550 ℃
=1.0

Modification factor: Size

The shaft diameter is 200 mm.  Therefore, the modification factor for size is:

Csize=1.0, if d≤8 mm1.189d-0.097,if 8 mm<d≤250 mm
=1.189×0.2-0.097
=0.71

Modification factor: Surface finish

From the graph, Csurf=0.7

Step 4: Formula for the S-N curve

The S-N curve is modeled by the following function:

σar,1N1b=σar,2N2b
N1N2b=σar,2σar,1
b=log10σar,2σar,1log10N1N2

The endurance at any completely reversed stress amplitude is then:

NR=σar,1σar1bN10.9fu≥σar≥Se∞σar<Se

For mean stress correction, Goodman was applied to calculate the equivalent completely reversed stress amplitude, σar from stress value with amplitude, σa, mean σm as follows:

σaσar+σmfu=1
σar=σa1-σmfu

These were programmed in the excel sheet below, from which the number of repetitions to failure is Bf=

# CLASS PROBLEM ON 2019-10-07

## Problem statement

The flange of a welded steel girder is classified as Detail category 125 according to BS EN 1993-1-9.  The component is subject to 500 000 cycles for stress range 200 MPa.  Adopt a safe life strategy with low consequence of failure.  The partial factor for equivalent constant amplitude stress range is γFf=1.0.  Is this design acceptable?

## Solution

Given is the following:

ΔσC=125 MPa
NC=2×106cycles

We need to modify this fatigue strength for temperature, post-weld treatment, corrosion, design philosophy, etc.  From the information given, we have only the design method.

Partial factor for fatigue

Specified is a safe life assessment method with low consequence of failure, for which γMf=1.15.

| Assessment method | Consequence of failure |  |
| --- | --- | --- |
|  | Low consequence | High consequence |
| Damage tolerant | 1.00 | 1.15 |
| Safe life | 1.15 | 1.35 |
| Source: BS EN 1993-1-9, 2005:11 |  |  |

Parameters on the SR-N curve

The reduced characteristic fatigue strength is:

ΔσC,red=ΔσCγMf

The constant amplitude fatigue limit is (no information was given on the SR-N curve slope, and it was assumed 3):

ΔσDm1ND=ΔσCγMfm1NC
ΔσD=ΔσCγMfNCND1m1
=1251.152513
=80 MPa

The stress range applied of 200 MPa, exceeds the constant amplitude fatigue limit, and, we have finite life.

To calculate endurance from S-N curve

The endurance on the SR-N curve is given as follows:

ΔσRm1NR=ΔσDm1ND, for 1.5fy>ΔσR≤ΔσD
ΔσRm2NR=ΔσDm2ND, for ΔσD>ΔσR≤ΔσL
Below ΔσL we have infinite life.

The endurance can now be calculated as follows:

NR=ΔσDΔσRm1ND 1.5fy>ΔσR≤ΔσDΔσDΔσRm2NDΔσD>ΔσR≤ΔσL∞ΔσR<ΔσL

Apply to the problem

For ΔσR=200 MPa and NR=500 000 cycles, the damage is:

- In this case the stress range is above the constant amplitude fatigue limit – finite life.

- The endurance at the supplied stress range is:

NR=ΔσDΔσRm1ND 1.5fy>ΔσR≤ΔσDΔσDΔσRm2NDΔσD>ΔσR≤ΔσL∞ΔσR<ΔσL
=8020035×106
=321 000 cycles

- The damage caused is: d1=n1N1=500000321000=1.56, this is larger than one, and we have failure.

The design is not sufficient.

# CLASS PROBLEM 2

## Problem statement

The fatigue performance of a welded detail in a steel linkspan structure can be represented by a fatigue curve corresponding to BS EN 1993-1-9 Detail Category 36.  The linkspan carries typical vehicles of weight 1, 2 and 5 ton.  A linear elastic finite beam element analysis revealed the stress ranges in the welded detail as summarised in the table on the right with the proportion of vehicles carried by the ferry 70%, 28% and 2% respectively as summarised in the table.  The linkspan is used twice per day.  No more than one vehicle can occupy the linkspan at any one time.  The design life required is equal to the service life of 40 years.  Is this design sufficient if a damage tolerant with high consequence of failure strategy is implemented?  A total of 50 vehicles are carried per day, and two stress cycles are caused to the linkspan per vehicle (on- and off loading).

## Solution

Partial factor for fatigue

Specified is a damage tolerant assessment method with high consequence of failure, for which γMf=1.15.

| Assessment method | Consequence of failure |  |
| --- | --- | --- |
|  | Low consequence | High consequence |
| Damage tolerant | 1.00 | 1.15 |
| Safe life | 1.15 | 1.35 |
| Source: BS EN 1993-1-9, 2005:11 |  |  |

Detail category fatigue curve

The problem specifies the fatigue curve as detail category 36.  Therefore, the unmodified fatigue strength at 2 000 000 cycles is 36 MPa.  We need to modify this value for modification factors and partial factor for fatigue.

Corrosive environment

Nothing is mentioned, it will be assumed that the linkspan is properly surface protected.

Modification factors

Nothing is mentioned about temperature and post-weld treatments, so all these factors will be excluded.

CT=1
CPWT=1

Constant amplitude fatigue limit

The constant amplitude fatigue limit in this case is:

ΔσD=ΔσCγMfNCND1m1
=23 MPa

There are stress ranges exceeding the constant amplitude fatigue limit, and therefore, we have finite life.

Cut-off limit

There are stress ranges below the constant amplitude fatigue limit, and therefore, the cut-off limit is required for calculation of endurance on this part of the curve.  The cut-off limit is:

ΔσL=ΔσDNDNL1m2
=13 MPa

Equation for endurance at any stress range

The endurance for corrosion protected or non-corrosive environment, is given as:

NR=ΔσDΔσRm1ND 1.5fy>ΔσR≤ΔσDΔσDΔσRm2NDΔσD>ΔσR≤ΔσL∞ΔσR<ΔσL

Apply to the problem

For ΔσR1=20 MPa and n1=1 022 000 cycles, the damage is:

The endurance is:

NR=ΔσDΔσRm1ND 1.5fy>ΔσR≤ΔσDΔσDΔσRm2NDΔσD>ΔσR≤ΔσL∞ΔσR<ΔσL
=232055 000 000
=10 200 000 cycles

The damage is then:

d1=n1NR1
=1 022 00010 200 000
=0.10

For ΔσR2=30 MPa and n2=408 800 cycles, the damage is:

The endurance is:

NR=ΔσDΔσRm1ND 1.5fy>ΔσR≤ΔσDΔσDΔσRm2NDΔσD>ΔσR≤ΔσL∞ΔσR<ΔσL
=233035 000 000
=2 272 400 cycles

The damage is then:

d2=n1NR1
=4088002 272 400
=0.18

For ΔσR3=40 MPa and n3=29 200 cycles, the damage is:

The endurance is:

NR=ΔσDΔσRm1ND 1.5fy>ΔσR≤ΔσDΔσDΔσRm2NDΔσD>ΔσR≤ΔσL∞ΔσR<ΔσL
=234035 000 000
=958 660 cycles

The damage is then:

d3=n3NR3
=29 200958 660
=0.0305

The total damage is then:

D=di
=0.10+0.18+0.03
=0.3106

The total damage is less than one and the design is sufficient.

Number of repetitions

The number of repetitions of the stress spectrum is:

Bf=1D
=3.22

Total design life

The design life of the linkspan is Period×Bf=PeriodD=3.22×40=129 years

# CLASS PROBLEM ON 2019-10-08

## Problem statement

- A fabricator of a pressure vessel elected to use as 25.4 mm plate made of:

  - Specify the material

- The radius should be 500 mm

- Determine the allowable working pressure of the cylindrical section of the pressure vessel

- Corrosion Allowance:

  - Make provision for 3.2 mm for corrosion

## Problem statement

In this case the shell thickness was prescribed.  Requested is the allowable working pressure of the cylindrical section of the pressure vessel.

Our approach can be as follows:

- Find the maximum allowable stress, S, for a plate material that include the thickness given.

- Calculate the internal diameter after corrosion occurred: D=2×500+2×3.2=

- Calculate the allowable working pressure

Material properties

From the material data sheet shown below, the material in Line 36 was chosen, it is plate product and covers the thickness range required as well as the operating temperature.  From this, the maximum allowable stress is:

S=103 MPa

Joint efficiency

In the absence of information on the weld quality control, it was decided to design the vessel as if made by single welded butt joints with backing strip with the limitations show in the Column3 of the table below.  The vessel will further be designed as no radiographic examination is done after completion of the welds.  For this, the joint efficiency is:

E=0.65

Calculate allowable working pressure

For a cylindrcal vessel under internal pressure, the maximum working pressure can be calculated by:

P=SEtr+0.6t
=103×0.65×(0.0254-0.0032)0.5+0.0032+0.6×(0.0254-0.0032)
=2.9 MPa

What will be the pressure be during the hydrostatic test at 1.3P:

σ=Pr+0.6ttE
=1.3×2.90.5+0.0032+0.60.0254-0.00320.0254-0.0032×0.65
=134 MPa

# THE REST OF THE PROBLEMS ARE FROM PREVIOUS LECTURES ON THE TOPIC  YOUR CLASSNOTES WILL BE UPDATED AFTER THE SECOND CLASS DAY

# S-N CURVE EXAMPLE

## Problem statement

Construct the S-N curve for a material with completely reversed stress amplitude σar1=500 MPa at Nf1=103 cycles and endurance limit σer=150 MPa at Nfe=106 cycles.  Then, calculate the endurance for the following completely reversed stress amplitudes: 300 MPa, 200 MPa, and, 100 MPa.

## Solution

The equation for the S-N curve is assumed to be: σ=ANfb.

Therefore:

A=σNfb
=σNf-b
σar1Nf1-b=σar2Nf2-b
Nf1Nf2-b=σar2σar1
b=-log10σar2σar1log10Nf1Nf2
=-0.1743

Say I need to calculate the endurance (fatigue life) at any stress amplitude, the equation becomes:

Nf1Nf2-b=σar2σar1
Nf1Nf2=σar2σar1-1b
Nfi=Nfeσerσari-1bσar103≥σari≥σer∞σari<σer

The other option is to find the equation for the S-N curve in the form σarmN=C.  For this, we use the points provided:

σar1mNf1=σar2mNf2
σar1σar2m=Nf2Nf1
m=log10Nf2Nf1log10σar1σar2

In this case, the endurance at any stress is then:

Nfi=Nfeσerσarimσar103≥σari≥σer∞σari<σer

From which it is clear that

m=-1b

# RAINFLOW COUNTING

The explanation that was done in class.

Table 1:  Rainflow counted stress spectrum over a period of 1 year

| σa | σm | Δσ | n |
| --- | --- | --- | --- |
| 45 | 35 | 90 | 0.5+0.5=1 |
| 90 | 10 | 180 | 0.5+0.5=1 |
| 25 | 25 | 50 | 0.5+0.5=1 |
| 35 | 25 | 70 | 0.5+0.5=1 |

(100;-80;180)

(80;-10;90)

(60;-10;70)

(50;0;50)

(-10;60;70)

(0;50;50)

(-80;100;180)

(-10;80;90)

Figure 1:  Stress signal over a period of 1 year

# BENDING MOMENT DISTRIBUTION

## Principle

Steps to calculate the bending moment at any position x:

- At position x, formulate the bending moments by just looking towards the origin of the coordinate system.

  - For x∈[0;a]:

My=MRA+Mw
=RAx-wx∙x2

  - For x∈[A;L]:

My=MRA+Mw
=RAx-wa∙x-a2

w

RA

x

z

x2

a

## Example

Consider the beam loaded in the -z direction with force 100 kN and constrained at Points A, B and C as shown in the figure below.  The bending moment distribution is also shown below.  From the bending moment distribution, if possible, the best point for splicing is where the bending moment is zero.

Point A

Point C

Point B

Figure 2:  Bending moment diagram

Figure 3:  Shear force diagram

# BENDING STRESS DISTRIBUTION

The bending stress distribution is given by:

σb,i=MxyiIxx-MyxiIyy
The second moment of area for this problem is:

Ixx=112WH3;Iyy=112HW3

For Point A:

σb,i=MxH2112WH3-MyW2112HW3
=6MxWH2-6MyHW2

If a tensile force is also applied, the stress at any point is given by:

σn=FA

Say a force of 1 kN is applied, what is the stress at point A?

# MEAN STRESS CORRECTION

## Problem Statement

Check sensitivity for the completely reversed bending stress amplitude, σar, for the mean stress of a signal using the following mean stress correction relationships:

- Modified Goodman

- Gerber

- Smith, Watson & Topper (WST)

- Walker

Assume a material ultimate tensile strength σu=700 MPa and consider the following stress states:

| Stress amplitude [MPa] | Stress mean [MPa] |
| --- | --- |
| 100 | -100 |
| 100 | 0 |
| 100 | 100 |

## Solution

From the notes, the relevant equations are:

| Approach | Equations |
| --- | --- |
| Modified Goodman | σar=σa1-σmσu |
| Gerber | σar=σa1-σmσu2, for σm≥0 |
| SWT | σar=σmaxσa =σmax1-R2 |
| Walker | σar=σmax1-γσaγ σmax>0 =σmax1-R2γ σmax>0 γ=-0.000200σu+0.8818(σu in MPa) |

Programmed in Excel, the results are as shown in the table below.  Can you explain and make recommendations?  See your text book.

# S-N CURVE STRESS LIFE EXAMPLE

## Problem statement

300WA structural steel has the following material properties:

E = 206 GPa, fy = 300MPa,

fut =450MPa

Assume a notch fatigue factor of kf=1.7

What is the endurance limit Psurv=0.5?

How many cycles to failure at

- σar1 = 200MPa

- σar2 =  300MPa

## Solution

Step 1:  Define the equation for the S-N curve

In this case the yield strength is below 700 MPa, and we will assume that the S-N curve need to be modified for a notch fatigue factor at 1 000 cycles.  For the general unmodified, unnotched material, the S-N curve has the following two points:

σar1mN1=σar2mN2
σar103m103=σerm106
However, we need to modify the S-N curve for the notch by the following factors:

Kf=1+Kt-11+ar=1.7

The notch fatigue factor at 1 000 cycles, Kf' is determined as Kf'=1 as shown below.

For Sut=64 ksi, Kf'-1Kf-1=0, therefore, Kf'=1

Figure 4:  Calculation of notch fatigue factor at 1 000 cycles

The limits on the S-N curve, modified for the notch, is:

σer=0.5σutKf
=0.5×4501.7
=132 MPa
σar103=0.9σut
=405 MPa

The equation for the S-N curve is now:

NR=σerσarRmNefor σarR≥σer∞for σarR<σer

Figure 5:  S-N curve for the notched specimen

The exponent (slope), m is:

σermNe=σar103m∙103
σerσar103m=103106
mlog10σerσar103=-3
m=-3log10σerσar103
=6.18

Step 2:  Calculate endurance at requested stress amplitudes

- For σar1=200 MPa (larger than σer), the endurance is:

N1=σerσar1mNe
=1322006.18∙106
=78 090 cycles

- For σar2=300 MPa (larger than σer), the endurance is:

N2=σerσar2mNe
=1323006.18∙106
=6 382 cycles

Step 3:  General remarks

If all the stress amplitudes where endurance was required are below the endurance limit, you do not need to model the S-N curve, because, the answer is infinite life.

# STRESS LIFE EXAMPLE WITH MEAN STRESS CORRECTION

## Problem statement

Component undergoes cyclic stress with:

σmax = 770MPa

σmin = 70MPa

Material is steel with σu = 1,050MPa and σer = 420MPa.  The fully reversed stress at σar103 = 770 MPa.

How many cycles can be loaded on the component until fatigue crack initiation?  That is, what is the fatigue life of the component?

## Solution

### Calculate stresses and compare with endurance limit

The stress amplitude is: σa=770-702=350 MPa

The mean stress is: σm=770+702=420 MPa

Do mean stress correction.  Use Goodman:

σaσar+σmσut=1
σar=σa1-σmσut
=3501-4201050
=583 MPa
The Goodman mean stress corrected equivalent completely reversed stress amplitude is σar=583≥420 MPa, therefore, we have finite life and the S-N curve must be calculated.

### S-N curve

The S-N curve is given as:

NR=σerσarRmNefor σarR≥σer∞for σarR<σer

For which:

σar103m∙103=σerm∙106
m=log10103106log10σerσar103
=11.4

### Calculate endurance at specified stress amplitude

σar=583 MPa is larger than the endurance limit σer=420 MPa.  For this completely reversed stress amplitude, the endurance is the:

NR=σerσarRmNer
=42058311.64∙106
=23 820 cycles

# FATIGUE: STRESS LIFE CALCULATION

## Solution

### Construct the S-N curve

From what we know, the fatigue strength of a mirror polished specimen subject to completely reversed bending, is as follows at 1 000 and 1 000 000 cycles:

σ103=0.9σu
σer=0.5σu

This is for 50% probability of crack initiation in endurance N

σer=CsizeCloadCsurfCTCrelσerb
Ce=CsizeCloadCsurfCTCrel
Ser=σerkf
=Ceσukf
S103=S103'CloadCTCrel

Modification factor: Notch

The fatigue notch factor at the endurance, or fatigue, limit is (note, this is at 1 000 000 cycles):

q=11+αρ
kf=1+kt-11+αρ
α=300fuksi1.8×10-3 in.

The fatigue notch factor at 1 000 000 cycles was calculated in the Excel sheet as Kf=1.98.

Fatigue notch factor at 1 000 cycles:

| q=Kf'-1Kf-1=ffut Kf'=qKf-1+1 =1.39 | ( | 51 | ) |
| --- | --- | --- | --- |

Figure 36:  Ration between notch fatigue factors at 1 000 and 1M cycles vs tensile strength

Modification factor:size

The modification factor for size was calculated from the following equation as 0.71 for the shaft with diameter 200 mm:

Modification factor: Load

The S-N curve was defined from a rotating bending test approach.  The loading is axial, and therefore, Cload=0.7.

Modification factor: surface

For the machined condition, Csurface=0.7

Modification factor: Temperature

The machine operates at 200 °C, where CT=1.0

CT=1.0 for T≤450 ℃1-5.8-3T-450, for 450<T≤550 ℃

Modification factor: Reliability

The S-N curve derived above, is for 50% probability of crack initiation (or survival).  The design requires a 1% probability of crack initiation (or 99% probability of survival).  From the table below, Crel=0.814 to achieve a probability of survival of 1% in N.

### Equation for the S-N curve

The S-N curve is modelled by the following function:

σ=ANfb
For which we have the following:

Ser=ANeb"
=A106b
S103=AN3b
=A103b

To solve:

SerS103=ANeb"AN3b
=NeN3b
b=log10SerS103log10NeN3
A=SerNeb

The endurance at any completely reversed stress amplitude, can be calculated as follows:

Ni=σarA1bfor σar≥Ser∞for σar<Ser

### Mean-stress compensation

The stress history has non-zero means.  Mean stress compensation using: Goodman, Morrow, SWT, Walker.

For Goodman: we already have ultimate strength.

For Morrow: Need σf, which is equal to A in this case, or, if the material was specified, it can be determined from the material data sheet.

For Walker, we need γ=-0.000200σu+0.8818(σu in MPa)

| Approach | Equations |
| --- | --- |
| Modified Goodman | σar=σa1-σmσu |
| Gerber | σar=σa1-σmσu2, for σm≥0 |
| SWT | σar=σmaxσa =σmax1-R2 |
| Walker | σar=σmax1-γσaγ σmax>0 =σmax1-R2γ σmax>0 γ=-0.000200σu+0.8818(σu in MPa) |

# STRAIN-LIFE EXAMPLE WITH STRAIN INPUTS

## Problem statement

The cyclic stress-strain and strain-life parameters for a steel is:

E=30 x 103 ksi; K’ = 154 ksi, σ’f = 133ksi, ε’f = 0.26, n’ = 0.202, b = -0.095,

c=-0.47

Determine the life for the histories shown on the next slide (use Morrow).

## Solution

The equations needed:

Ramberg-Osgood: ε=σE+σH'1n'

Strain-life equation: ε=σf'E2Nfb+εf'2Nfc

See the attached Excel spreadsheet.

# DAY 2: YOUR FIRST DAMAGE CALCULATION

## Problem Statement

Component undergoes axial cyclic stress as follows:

Table 2:  Stress spectrum for one block

Material is steel with Sut = 1,050MPa with hardness 350 BHN.  The theoretical stress concentration factor at a notch on the part is Kt=2.  The notch radius is r=4 mm.  The surface finish is machined.  The shaft has a radius of 100 mm and operates at temperature T=200 °C.

How many blocks of loading can be loaded on the component for a 1 % probability of fatigue crack initiation?  That is, what is the fatigue life of the component?

## Solution

The steps that I will follow:

- Calculate notch fatigue factors:

- Calculate the influencing factors and the fatigue strength at 1 000 and 1 000 000 cycles as shown below:

Se=Se'CsizeCloadCsurfCTCrel
=0.5SutKfCsizeCloadCsurfCTCrel
S103=S103'CloadCTCrel
=0.9SutKf'CloadCTCrel

- Mean stress correction to calculate the equivalent completely reversed stress amplitude.  Use Goodman:

Sa=σa1-σmSut

- Calculate damage using the Palmgren-Miner rule

D=niNi

- Calculate life which is:

Life=Period of stress spectrumD

### Calculate the S-N curve, modified for applicable effects

#### Modification factors

The modification factors affect the fatigue strength at 103 and 106 cycles as follows:

S103*=0.9Sut
Se*=0.5Sut
S103=S103*CTCrelCloadCsize
Se=Se*CTCrelCloadCsurfCsize

Modification factor: Temperature

We operate at 200 °C.  Roymech recommends the following modification for temperature:

CT=1.0 for T≤450 ℃1-5.8-3T-450, for 450<T≤550 ℃

In this case, at 200 °C, CT=1.0.

Modification factor: Reliability

The standard S-N curve is constructed, normally from a completely reversed test, for a 75% confidence level of 50% probability of survival in N.  It was requested to perform that fatigue calculations for a probability of survival of 99% (or 1% probability of crack initiation).  From Table 2 the modification factor for reliability is then Cr=0.814.

Table 3:  Reliability modification factors

Modification factor: Load

No information was provided for loading.  Therefore, it was assumed that Cload=1.  If, it was mentioned that the component is subject to a normal stress, the load modification factor would have been Cload=0.70.

A conservative relationship due to the volume subject to high stress in the axial stress state relative to the bending stress used to construct the S-N is as follows, from which it is clear that in this case Cload=0.7:

| Se,axial=0.70Se,bending Cload=0.7 if S-N curve is from bending tests |  |  |  |
| --- | --- | --- | --- |

Modification factor: Surface finish

The standard S-N curve is from mirror polished specimens.  In this case, the surface is machined, and, from Figure 5 the modification factor for surface finish is Csurf=0.7 at ultimate tensile stress Sut=10507=150 ksi.

Figure 6:  Surface finish modification factors

Modification factor: Size

The recommended modification factor for size is:

Csize=1.0, if d≤8 mm1.189d-0.097,if 8 mm<d≤250 mm

In this case, the component diameter is D=2×100=200 mm.  The modification factor for size is then:

Csize=1.189d-0.097
=1.189200-0.097
=0.71

Modification factor: Fatigue notch factor at 106 cycles

The fatigue notch factor at 106 cycles will be calculated from:

Kf=1+Kt-11+ar
a=300fuksi1.8×10-3 in.

Modification factor:  Fatigue notch factor at 103 cycles

The notch fatigue factor at 1 000 cycles is calculated from the following formula:

Kf'-1Kf-1=q

Where q=0.4 for the 1 050/7=150 ksi steel as shown in the figure below.  Therefore:

Kf'=qKf-1+1

For the assumed yield strength of 800 MPa, the fatigue notch factor at 103 cycles is calculated as follows:

Kf'-1Kf-1=0.4
Kf'=0.4Kf-1+1

For Sut=10507=150 ksi, Kf'-1Kf-1=0.4

Figure 7:  Calculation of notch fatigue factor at 1 000 cycles

### The equation for the S-N curve

The slope of the S-N curve is given as follows:

S103m103=Sem106
m=log10103log10S103Se
=3log10S103Se

The endurance at any completely reversed stress amplitude is:

NR=SeSRmNefor SR≥Se∞for SR<Se

### Calculations

For the supplied stress spectrum, the life is 12 Blocks for a 1% probability of failure (99% probability of survival).

Table 4:  Stress spectrum for one block

### What if the stress was normal?

When a normal stress is applied, and the S-N curve is for reversed bending, the modification factor for load is Cload=0.70.  For this case, the life is 1 Blocks for 99% probability of survival as shown below.

Table 5:  Stress spectrum for one block (with load modification factor)

# EXAMPLE 2 IN THE NOTES

## Problem statement

## Solution

### Step 1: Define the fatigue curve

The modified characteristic strength at 2 million cycles is given by:

ΔσC=36γMFCtemp

The design requires damage tolerant design with low consequence of failure, that means γMF=1.15.

For temperature, the modification factor at 300 °C is Ctem=0.85.

The modified characteristic strength is then:

ΔσC=361.150.85
=26.6 MPa

The constant amplitude fatigue limit is:

ΔσD=ΔσCNCND1m
=2513ΔσC
=0.74ΔσC
=19.7 MPa

The cut-off limit is:

ΔσL=0.41ΔσC
=10.8 MPa

### Endurance calculation

There are stress ranges exceeding the constant amplitude fatigue limit, therefore, finite life and the Sr-N curve is given by:

NR=ΔσCΔσRm1NCm1=31.5fy≥ΔσR≥ΔσDΔσDΔσRm2NDm2=m1+2ΔσD≥ΔσR≥ΔσL∞ΔσL>ΔσR

For Δσ=20 MPa

NR1=19.7203×5E6
=4 778 358
d1=1 022 0004 778 358
=0.21

# THIN WALL PRESSURE CYLINDER

The force that holds the longitudinal loads:

Cross-section area of steel: A=πDt
Area of pressure force: FP=π4D2P
Stress produced in steel:

σA=Fp=π4D2P
σ=π4D2πDtP
=DP4t

# PRESSURE VESSEL DESIGN EXAMPLE

## Problem statement

## Solution

### Material selection

Choose plate steel to SA2062.  Line 23 below.

The allowable stress at the operating temperature, assume room temperature, is: S=117 MPa.

### Joint efficiency

Assume no radiography.  Assume welds are all butt welds according to the description below, from which the joint efficiency is E=0.7.

### Thickness to use in calculation of design pressure

The thickness of 25.4 mm plate, specified by the client, includes a corrision allowance of 3.2 mm.  Therefore, the thicknes to use in the determining the design pressure shall be 25.4-3.2=22.2 mm

### Maximum allowable operating pressure

We know that the longitudinal (Category A) welds are loaded to the highest stress.  Or, in other words, the circumferential stress will govern the maximum allowable pressure.

The maximum allowable operating pressure:

P=SE1tr+0.6t
=117×0.7×22.2500+0.6×22.2
=3.5 MPa

# Acceptable fatigue design question

## Problem Statement

The flange of a welded steel girder is classified as Detail category 125 according to BS EN 1993-1-9.  The component is subject to 500 000 cycles for stress range 200 MPa.  Adopt a safe life strategy with low consequence of failure.  The partial factor for equivalent constant amplitude stress range is γFf=1.0.  Is this design acceptable?

## Solution

Partial factor for fatigue:

From the table below, the partial factor for fatigue strength for safe life and low consequence of failure is γMf=1.15.

Modification factors

No modification effects requested.  So, none applicable.

Fatigue curve

For the stress range given above, the S-N curve equations can be manipulated as below to calculate the endurance at any stress range:

NR=ΔσcγMfΔσR 3Nc=1251.1520032×106=321 000 cycles.  Therefore, the endurance at 200 MPa is 321 000 cycles, which is below the  required 500 000 cycles, and, the design do not comply.

ALTERNATIVELY

ΔσC=125 MPa

Steps:

- Calculate the stress range at 500 000 cycles, for the partial factor for fatigue modified Sr-N curve.

- Check if the applied stress range is below the stress range calculated above, if so, the design is acceptable.

Could also:

- Calculate the endurance at stress range 200 MPa from the partial factor modified Sr-N curve.

- If the applied number of cycles is < than this endurance, the design is acceptable.

Modification factors

In this case we only need to modify for the safe life strategy with high consequence of failure, for which γMf=1.15.

### Check 1

The stress range that the Sr-N curve allows at endurance 500 000 cycles is:

ΔσR=ΔσCγMf∙NCNR1m1

Assume the slope of the Sr-N curve is m1=3.

Therefore:

ΔσR=1251.152×10650000013
=172 MPa

This stress range is BELOW the applied stress range, and the design is not acceptable.

### Check 2: Calculate endurance

The endurance NR at 200 MPa stress range is 321 000 cycles, which is less than the required 500 000 cycles and the design is not acceptable:

NR=ΔσCγMfΔσRm1NC
=1251.152003×2×106
=321 000 cycles

# WELD FATIGE EXAMPLE ON 2017-08-15

## Problem statement

The fatigue performance of a welded detail in a steel linkspan structure can be represented by a fatigue curve corresponding to BS EN 1993-1-9 Detail Category 36.  The linkspan carries typical vehicles of weight 1, 2 and 5 ton.  A linear elastic finite beam element analysis revealed the stress ranges in the welded detail as summarised in the table on the right with the proportion of vehicles carried by the ferry 70%, 28% and 2% respectively as summarised in the table.  The linkspan is used twice per day.  No more than one vehicle can occupy the linkspan at any one time.  The design life required is equal to the service life of 40 years.  Is this design sufficient if a damage tolerant with high consequence of failure strategy is implemented?  A total of 50 vehicles are carried per day, and two stress cycles are caused to the linkspan per vehicle (on- and off loading).

The exhaust pipe blows are at temperature 350 °C on the link.  No post-weld treatment was done, as it was reserved for when failures occur.

## Solution

### Steps

The following steps will confirm the design:

- Calculate the partial factor for fatigue.

- Calculate temperature modification factor.

- Calculate total damage and fatigue life.

### Partial factor for fatigue

For a damager tolerant and high consequence of failure strategy, the partial factor for fatigue is γMf=1.15.

### Temperature modification factor

The modification factor for temperature for operating at 350°C is CT=0.79.

CT350°C=0.79

### Equation for the S-N curve

The endurance is given as follows:

NR=Δσc'ΔσRm1Ncfor ΔσD≤ΔσR≤1.5fyΔσDΔσRm2NDfor ΔσL≤ΔσR≤ΔσD∞for ΔσR≤ΔσL

The important points on the S-N curve is then:

ΔσD=ΔσcγMf×CT NcND13=18.2 MPa
ΔσL=ΔσDNDNL15=10 MPa

### Damage calculation

For 20 MPa:

NR=ΔσDΔσRm1ND=18.22035×106=3 781 248

D20=1 022 0003 781 248=0.27

For 40 MPa:

NR=470 981
D40=0.87

For 100 MPa:

NR=30 249
D100=0.97

The total damage is then:

The total damage is then:

DT=D20+D40+D100
=2.11

Therefore the design life of the link for the specified stress spectrum is:

DesLife=402.11
=20 years

### The stress spectrum

To calculate the applied cycles over the design life of 40 years, the following formula was used:

ni=50×2×365×40×Pi

## Steps

- Construct the Sr-N cure.  Modify for

  - Partial fatigue strength factor, γMf.

  - Temperature.

  - Post-weld treatment.

- Calculate damage.

- Calculate life.

- Make recommendations on the use of post—weld treatments if the fatigue life is < design life required.

## Calculate damage

The equation of the Sr-N curve that will be used to calculate endurance, is as follows:

NR=ΔσC,modΔσRm1NC for ΔσD≤ΔσR<1.5SyΔσDΔσRm2NDfor ΔσL≤ΔσR<ΔσD∞for ΔσR<ΔσL

## What about post-weld treatment

The first to verify, is if the post-weld treatment will be of any benefit for the detail.

When we do peening.

- Special requirements

  - Maximum of nominal compressive stress including proof loading <0.25fy

    - Assume we comply

  - Dependent on stress ratio:

    - R<0 effective stress range = Δσ

    - 0<R≤0.4 effective stress range = maximum applied stress σ

    - R>0.4 no benefit

It is assumed that the link is only loaded on one direction, from zero stress to a maximum value equal to the range.  In this case R=0.  Therefore, the effective stress range is as given in the table.

Assume the material is structural steel 350W.  For this material, the benefit from peening is as follows:

Benefit=1.3ΔσC with maximum 112 MPa

# WELD FATIGE CLASS PROBLEM INCLUDING ALL

An 8 mm double fillet weld was used in a T-joint as shown below.  The stress spectrum was calculated over a period of 5 years and is summarized in the table below.  The surface is corrosion protected.  The component operating temperature is at 250 °C.  Because of the small weld that was used in the construction, the weld toes were burred to specification, and peened to specification afterwards.  The stress range has in all cases a stress ratio of R=-0.2.  The component was heat treated before post-weld treatment.  The design strategy is damage tolerant with low consequence of failure.  What is the fatigue life of the component?

Table 6:  Stress spectrum over a period of 5 years

Δσ

50

50

Width: w=200

## Solution

The following procedure will be used:

- Find the partial factor for fatigue.

- Calculate modification factors:

  - Temperature.

  - Size.

  - Post-weld treatment.

  - Heat-treatment effects.

- Determine detail categories.

- Determine the equation for the S-N curve for crack initiation at the:

  - Weld toe.

  - Weld root.

- Calculate damage.

- Calculate life.

### Partial factor for fatigue

For a damage tolerant and low consequence of failure, the partial factor for fatigue is γMf=1.0.

### Modification factors/effects

#### Temperature

The modification factor for operation at 250 °C is CT=0.9.

### Detail category: crack initiation at the weld toe

The detail category for crack initiation at the weld toe is ΔσCtoe=71.  This detail will benefit from heat treatment, weld toe treatment, and, peening.

### Detail category: crack initiation in the weld root

In this case, the detail category is marked with an *, and can be moved one category up.  In this case conservativeness is not so important and the detail category was raised by one level to ΔσCthroat=40 (see S-N curves below).  This detail will NOT benefit from weld toe treatment or peening.  But, it will benefit from heat treatment.

### Heat treatment

In this case heat treatment allows the use of 60% of the compressive part in the stress signal for range calculation.  The stress spectrum only provides the stress range and stress ratio.  To calculate the compressive stress and effective stress range for every given stress range, the following equation was used:

R=σminσmax
RHT=0.6σminσmax=0.6R
σmin=Rσmax
Δσ=σmax-σmin
=σmax(1-R)

Steps to follow:

- Calculate σmax=Δσ1-R

- Calculate new stress range from: ΔσHT=σmax1-RHT=Δσ×1-RHT1-R

### Grinding and peening for improvement at the weld toe

The problem statement mentioned grinding, then peening afterwards.  In this case, we can have the benefit of both provided that we do not exceed the limits as specified.

#### Grinding

For toe grinding the benefit and finale characteristic strength is:

ΔσCg=min1.3ΔσC112

#### Peening

The benefit from peening after grinding is:

ΔσCp=min1.3ΔσCg112

### Stress in the weld throat

The stress in the weld throat from the nominal stress as given will be calculated as follows:

Δσwaww=Δσtw
Δσw=Δσtaw

### Damage calculation and fatigue life assessment

The equation for the S-N curve will calculated endurance for any stress range as follows:

NR=ΔσDΔσRm1NDfor ΔσD≤ΔσR≤1.5fy, m1=3ΔσDΔσRm2NDfor ΔσL≤ΔσR<ΔσD, m2=5 ∞for ΔσR<ΔσL

### Fatigue life for crack initiation at the weld toe

The fatigue life for 95% probability of survival for crack initiation at the weld toe is 16.9 years.

### Fatigue life for crack initiation at the weld throat

The fatigue life for 5% probability of crack initiation in the weld throat is 2.16 days!  Please redesign this thing.

# PRESSURE VESSEL EXAMPLE 1

## Problem statement

- A fabricator of a pressure vessel elected to use as 25.4 mm plate made of:

  - Specify the material

- The radius should be 500 mm

- Determine the allowable working pressure of the cylindrical section of the pressure vessel

- Corrosion Allowance:

  - Make provision for 3.2 mm for corrosion

Answer in class in the class notes document

## Solution

Methodology:

- Select a material that can handle the operating temperature and environment.

- Assume no non-destructive testing.  Find joint efficiency for category A welds with no NDT.

- Calculate a thickness of t=25.4 – 3.2.

- Calculate pressures for this t.

### Select material

No temperature was specified and it is assumed that the vessel will operate under room temperature.  The selection of the material was done as follows:

- Selected materials that can offer a wide thickness range.  I can always iterate this process if the plate selected now is not the best option.

- Confirmed that the material can be used at the operating temperature.

This resulted in the selection of the following material:

SA-537 Plate, S = 20 ksi at room temperature

The maximum allowable stress on this material at room temperature is 140 MPa.

### Joint efficiency

The circumferential stress is the highest.  Therefore, joint efficiencies for Joint A is required.  No information on the welds were given.   An instruction will be given for the WPS to specify a welding from one side without a backing strip.  For this weld with no post-weld NDT, the joint efficiency is E=0.6.

## Applicable equations

From the table below, the pressure for the cylindrical shell is given by (the thickness t=tplate-tcorrosion):

P=SEtr+0.6t
=140∙0.6∙0.02220.5+0.6∙0.0222
=3.6 MPa

# PRESSURE VESSEL AND CHECK FOR BUCKLING

## Problem statement

- A horizontal vessel with inside diameter 1,500 mm is to be fabricated from SA-516 Grade 70 material.  The design pressure at the top of the vessel is 3,378 kPa (3.4 MPa) at 216 °C.   This measurement point was at a height of 1.5 m above the centerline of the cylinder.

  - All longitudinal joints shall be Type 1 and spot radiographed in accordance with UW-52

  - Circumferential joints are Type 1 with no radiography

- Vessel operates full of liquid with density 998 kg/m3.  Distance from the centerline to the uppermost part of vessel is 1.5 m.

- Determine the required thickness at Point A

  - Neglect the weight of the vessel in the calculation

- UG-22 states that the static head of the liquid must be included in the pressure P

## Solution

- Calculate the design pressure.

- Find the maximum allowable design stress.

- Circumferential stress

  - Find joint efficiency.

  - Calculate t

- Longitudinal stress at the bottom

  - Find joint efficiency

  - Calculate bending stress

  - Calculate t

  - Calculate stress at the top of the vessel.

    - If < 0, check for buckling.

- Add thickness for corrosion

### Design pressure

The pressure at the top of the vessel was given 3 378 kPa.  However, hydrostatic pressure need to be included and from this the design pressure is:

P=3 378×103+ρgh
=3 378×103+998×9.81×2.25
=3.4 MPa

### Maximum allowable design stress

The temperature is 443 °F.  For this, the maximum allowable stress is 20 ksi, 140 MPa.

### Circumferential stress

#### Joint efficiency and thickness

The joint efficiency for the longitudinal welds is E=0.85.  The thickness required is:

t=PrSE-0.6P
=3400×0.75140000×0.85-0.6×3400
=21.8 mm

Confirm that this thickness is available for the material.

### Longitudinal stress at the top

The longitudinal stress due to pressure and bending is given by the following equation:

σtop=MyI+PR+0.2tt
=-WL2Ro8∙π4Ro4-Ri4+PRi+0.2tt

=-3.4 MPa  Ag nee, this is tto small to demonstrate buckling.  Say it is:
=-80 MPa

The maximum bending moment is at the centre of the pressure vessel:

M=WL28
W=9.81×998πr2
L=303.3=9 m

P=2SEtR+0.2t
SE=PR+0.2tt

There is compressive stress.  Confirm buckling.

### Confirm buckling

Step 1:  Calculate A

A=0.125Rot
=0.0034

Step 2:  Factor B from graph

From the graph below, the factor is B=12.400 ksi ~100 MPa.  Therefore, the thickness is adequate to prevent buckling because B=100 MPa is more than the compressive stress of 80 MPa.

### Check longitudinal stress at bottom

σb=WL2Ro8∙π4Ro4-Ri4
=3.6 MPa

This is small contribution and will be neglected.

# PLANE STRESS AND STRAIN

The constitutive model for isotropic materials:

εx=σxE-νEσz+σy
εy=σyE-νEσz+σx
εz=σzE-νEσx+σy

Say we have stress state: σx=1, σy=0 and σz=0

Under plane strain conditions, the strains εy=ε-z=0.  Then stresses σy and σz will be generated because:

εx=σxE-νEσz+σy
0=σyE-νEσz+σx
0=σzE-νEσx+σy

# FRACTURE MECHANICS

# FRACTURE MECHANICS CLASS PROBLEM

## Problem statement

You have a rectangular cross section steel part with yield strength 500 MPa and Charpy test energy 35 J that has a double edge crack measured 2 mm on each side.  The part is subject to a axial stress amplitude 100 MPa, mean 0 MPa, for 50 cycles per hour.  The width of the part is 250 mm and thickness is 30 mm.  The part is used for 8 hours per day.  For how long can the part be used before failure?  What can be done to increase the fatigue life.

## Solution

Steps:

- Determine the plane strain fracture toughness of the material.

- Calculate the crack size where failure occur.

  - Fracture

  - Plastic collapse

- Get a model for the geometric stress concentration factor.

- Set up the Paris rule for crack propagation.

- Solve

### Plane strain fracture toughness

A lower bound for the plane strain fracture toughness will be used, given by:

KIc=21.6Cv0.17  MPam

### Fracture

Fracture occurs when the crack size reaches a value so that the stress intensity factor equals the plane strain fracture toughness at the maximum tensile stress:

KI=βaσπa
afr=1πKICβafrσmax2

The geometric stress concentration factor is given by the following figure:

### Plastic collapse

Plastic collapse occurs when the crack size reaches a value so that the stress in the remaining section becomes equal to the yield strength:

σrem=FnomBW-2a
=σnomWBBW-2a
SyW-2acol=σnomWBB
W-2acol=σnomWBBSy
2acol=W-σnomWBBSy
acol=12W-σnomWBBSy

### Crack propagation

The crack propagation will be modelled as follows:

dadN=CΔK+m
where

C=1×10-8
m=3

## Calculation sheet

For this load application the stress ration is -1.  Therefore the threshold stress intensity level is 5.4 MPam0.5.  The applied stress intensity range is 8.9 MPam0.5, which is higher than threshold value, and, crack propagation will occur.  From the table below, the crack will propagate to 36 mm in 450 cycles where the fracture toughness is reached.  The component fails in fracture.  For fracture collapse, a material with plane strain facture toughness of 70 MPam0.5 or more is required to allow the crack to grow to 100 mm in length.

Life can be extended by:

- Repairing the crack.

- Drill-stop the crack.

- Retard the crack by tensile overloading.