# INTRODUCTION

This document will be updated with the notes made during class.  The document will be made available in MS WORD format to allow students access to the Excel spreadsheets that were included during class.  Please note that this document was compiled during class and was not proof read for typing, language, and calculation errors.  Please inform the lecturer should you detect any serious errors.

# LINKS

https://wits2020.s3.amazonaws.com/Wits+2020+Weld+Fatigue+-+Introduction+-+1+Study+Guide.mp4

https://wits2020.s3.amazonaws.com/Wits+2020+Weld+Fatigue+-+Introduction+-+2+Website.mp4

# BENDING STRESS ON SQUARE CROSS-SECTION

## Problem statement

## Solution

The second moments of area for the cross section are:

Ixx=112WH3
Iyy=112HW3

W=0.050;H=0.100;Ixx=1/12*H*W^3,Iyy=1/12*W*H^3,

Ixx =   1.0417e-06

Iyy =   4.1667e-06

The bending stress at any location in the x-y plane is:

σb,i=MyxiIxx-MxxiIyy

sigb=Mx*xy(:,2)/Ixx-My*xy(:,1)/Iyy

sigb = 1.0e+07 *[0.9600 -0.9600 1.200]

# BENDING MOMENT DISTRIBUTION

## Principle

Steps to calculate the bending moment at any position x:

- At position x, formulate the bending moments by just looking towards the origin of the coordinate system.

  - For x∈[0;a]:

My=MRA+Mw
=RAx-wx∙x2

  - For x∈[A;L]:

My=MRA+Mw
=RAx-wa∙x-a2

w

RA

x

z

x2

a

## Example

Consider the beam loaded in the -z direction with force 100 kN and constrained at Points A, B and C as shown in the figure below.  The bending moment distribution is also shown below.  From the bending moment distribution, if possible, the best point for splicing is where the bending moment is zero.

Point A

Point C

Point B

Figure 2:  Bending moment diagram

Figure 3:  Shear force diagram

# BENDING STRESS DISTRIBUTION

The bending stress distribution is given by:

σb,i=MxyiIxx-MyxiIyy
The second moment of area for this problem is:

Ixx=112WH3;Iyy=112HW3

For Point A:

σb,i=MxH2112WH3-MyW2112HW3
=6MxWH2-6MyHW2

If a tensile force is also applied, the stress at any point is given by:

σn=FA

Say a force of 1 kN is applied, what is the stress at point A?

# TOTAL SHEAR STRESS IN THE THROAT OF A WELD

## Problem Statement

Calculate the total shear stress (due to shear and normal stress) at Point A on the cross-section for a 203x133x30 parallel flange I-section subject to the simultaneous loads given below:

| Load | Unit | Value |
| --- | --- | --- |
| Fx | N | 5 000 |
| Fy | N | 1 000 |
| Mz=T | Nm | 500 |

The beam length is 3 m and the weld size is e=8 mm (throat size a=5.7 mm).

Point A

Table 1:  Properties of cross-sections

## Solution

### Calculate the cross-section properties

A sketch of the weld cross-section is shown below.

tf

tw

h

b

A=a2b+4tf+2h-2tf+2b-tw
=.00533748 m4
Ixx=2112ah-2tf3+2ab-twh2-tf2+4atfh2-tf22
=2.1188707052e-05 m4
Iyy=2(ah-2tftw22+2112ab3+4atfb22+2112ab3-tw3
=5.5406317145e-06 m4
Izz=Ixx+Iyy=2.67293387665e-05  m4
h=206.8 mm;b=133.9 mm;tw=6.4 mm;tf=9.6 mm

x

y

The coordinates for Point A is (x; y) = b2;h2=(0.067; 0.103).

### Calculate stress due to axial load

σn=FxA
=5 0000.00533748
=0.9 MPa

### Calculate bending stress at Point A

Mx=FyL
=1 000×3
=3 000 Nm

The bending stress is given as:

σb=MxyIxx-MyxIyy
=14.6 MPa

The total axial stress at Point A is then

σa=15.5 MPa

### Shear stress due to shear forces

We are evaluating stress at the corner, where there is no shear stress due to shear forces.

### Shear stress due to torque

In the x-direction

τx=-Th2Izz
=-1.9 MPa

In the y-direction

τy=Tb2Izz
=1.3 MPa

### The total shear stress

τ=τx2+τy2+σa2
=1.92+1.32+15.52
=15.7 MPa

# RAINFLOW COUNTING EXPLAINED

Please watch the videos referenced in your notes.

The remainder of this section presents the counting that was demonstrated in class.  A video of this presentation is:

| # | Stress from | Stress to | ni | σa | σm | Δσ |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 190 | -175 | 0.5 |  |  |  |
| 2 | -125 | -50 | 0.5 | 37.5 | -87.5 | 75 |
| 3 | -50 | -125 | 0.5 | 37.5 | -87.5 | 75 |
| 4 | -175 | 120 | 0.5 | 147.5 | -27.5 | 295 |
| 5 | 120 | -175 | 0.5 | 147.5 | -27.5 | 295 |
| 6 |  |  |  |  |  |  |
| 7 |  |  |  |  |  |  |
| 8 |  |  |  |  |  |  |

10

9

8

7

6

5

4

3

2

1

| # | Stress from | Stress to | ni |
| --- | --- | --- | --- |
| 1 |  |  |  |
| 2 |  |  |  |
| 3 |  |  |  |
| 4 |  |  |  |
| 5 |  |  |  |
| 6 |  |  |  |
| 7 |  |  |  |
| 8 |  |  |  |

# STRESS-LIFE PROBLEM

## Problem statement

Component undergoes axial cyclic stress as follows, which was obtained by Rainflow counting of the stress signal for one repetition OF 3 months.

| Stress amplitude [MPa] | Stress mean [MPa] | Number of cycles/repetition |
| --- | --- | --- |
| 100 | 00 | 10000 |
| 50 | 0 | 5000 |
| 100 | 100 | 20000 |
| 200 | -100 | 2000 |

Material is steel with Sut = 1,050 MPa with hardness 350 BHN.  The theoretical stress concentration factor at a notch on the part is Kt=2.  The notch radius is r=4 mm.  The surface finish is machined.  The shaft has a radius of 100 mm and operates at temperature T=500 °C

How many repetitions of loading can be loaded on the component for a 1 % probability of fatigue crack initiation?  That is, what is the fatigue life of the component?

## Solution

### Notched specimen – calculate the fatigue notch factors

At 106 cycles

The fatigue notch factor is given by the following equation:

Kf=σerbun-notchedσerbnothced
Kf=1+Kt-11+αr

Peterson for steels (Dowling, 2013, p. 498):

logα=2.654×10-7σu2-1.309×10-3σu+0.01103

α in mm=10logα  345≤σu≤2 070 MPa
=102.654×107σu2-1.309×103σu+0.01103

So, for this problem we have for an ultimate tensile strength 1 050 MPa:

α=102.654×10-7σu2-1.309×10-3σu+0.01103
=102.654×10-7∙10502-1.309×10-3∙1050+0.01103
=0.085 mm

From this, the fatigue notch factor at one million cycles is:

Kf=1+Kt-11+αr
=1+2-11+0.0854
=1.98

AT 1 000 cycles

For the ultimate tensile strength 152 ksi, the notch sensitivity factor from the figure is q=0.43, for which:

Kf'-1Kf-1=fσu=q=0.43
Kf'=qKf-1+1
=0.431.98-1+1
=1.42

The S-N curve modified for the notch, will then have the following strengths at 1 000 and 1 000 000 cycles:

σer=σerb'CsizeCloadCsurfCTCrel
σerb'=σerbKf
σar,103=σarb,103'CloadCTCrel
σarb,103'=0.9σuKf'

From these we have:

σer=0.5σuKfCsizeCloadCsurfCTCrel
σar,103=0.9σuKf'CloadCTCrel

### Modification factors

#### Load

In this case the specimen will be subject to an axial load, while the fatigue S-N curve is for a rotating bending test (note, always check for vice-versa).  Therefore, modification factor for load is:

Cload=0.7

#### Temperature

The component will be operated at 500 ℃, for which the modification factor for temperature is:

CT=1.0 for T≤450 ℃1-5.8-3T-450, for 450<T≤550 ℃
=1-5.8-3500-450
=0.74

#### Reliability

The design must be made for 1% probability of failure, or 99% probability of survival.  Therefore, from the table below, Crel=0.814.

#### Surface

For the machined surface, the surface roughness modification factor is Csur=0.7.

#### Size

A size modification factor is shown below, from which (for a diameter of 200 mm):

Csize=1.0, if d≤8 mm1.189d-0.097,if 8 mm<d≤250 mm
=1.189200-0.097
=0.71

#### Construct the fatigue curve

The fatigue curve, modified for the notch and the environmental factors, has the following strengths at 1 000 000 and 1 000 cycles respectively:

σer=0.5σuKfCsizeCloadCsurfCTCrel
=0.5×1 0501.98∙0.71∙0.70∙0.70∙0.74∙0.814
=55.6 MPa
σar,103=0.9σuKf'CloadCTCrel
=0.9×1 0501.42∙0.70∙0.74∙0.814
=280.6 MPa

The S-N curve from 1 000 cycles to 1 000 000 cycles will be modelled by the following equation:

σar,1mN1=σar,2mN2
m=logN2N1logσar,1σar,2
=log106103log280.655.6
=4.27
Now, the endurance at any completely reversed stress amplitude can be calculated from the following equation:

NR=σar,1σarmN10.9σu≥σar≥σer∞σar<σer

### Mean stress correction

The supplied stress spectrum has non-zero mean stresses.  The Goodman equation will be applied to calculate the completely reversed stress amplitude as follows:

σaSa,r+σmσu=1
Sa,r=σa1-σmσu

### Calculate damage

| Stress amplitude [MPa] | Stress mean [MPa] | Number of cycles/repetition |
| --- | --- | --- |
| 100 | 00 | 10000 |
| 50 | 0 | 5000 |
| 100 | 100 | 20000 |
| 200 | -100 | 2000 |

For σa=100 MPa and σm=0 MPa, applied for 10 000 cycles, we have:

- The completely reversed stress amplitude is 100 MPa.

- This exceeds the endurance limit of 55.6 MPa.

- The endurance is

NR=σar,1σarmN10.9σu≥σar≥σer∞σar<σer
=55.61004.27106
=81 558 cycles

- The damage is:

d1=10 00081 558
=0.123

| Stress amplitude [MPa] | Stress mean [MPa] | Number of cycles/repetition |
| --- | --- | --- |
| 100 | 00 | 10000 |
| 50 | 0 | 5000 |
| 100 | 100 | 20000 |
| 200 | -100 | 2000 |

For σa=50 MPa and σm=0 MPa, applied for 5 000 cycles, we have:

- The completely reversed stress amplitude is 100 MPa.

- This is less than the endurance limit of 55.6 MPa.

- The endurance is

NR=σar,1σarmN10.9σu≥σar≥σer∞σar<σer
=∞

- The damage is:

d2=5 000∞
=0

| Stress amplitude [MPa] | Stress mean [MPa] | Number of cycles/repetition |
| --- | --- | --- |
| 100 | 00 | 10000 |
| 50 | 0 | 5000 |
| 100 | 100 | 20000 |
| 200 | -100 | 2000 |

For σa=100 MPa and σm=100 MPa, applied for 20 000 cycles, we have:

- The completely reversed stress amplitude is:

Sa,r=σa1-σmσu
=1001-1001 050
=110.5 MPa

- This exceeds the endurance limit of 55.6 MPa.

- The endurance is

NR=σar,1σarmN10.9σu≥σar≥σer∞σar<σer
=55.6110.54.27106
=53 249

- The damage is:

d3=20 00053 249
=0.376

| Stress amplitude [MPa] | Stress mean [MPa] | Number of cycles/repetition |
| --- | --- | --- |
| 100 | 00 | 10000 |
| 50 | 0 | 5000 |
| 100 | 100 | 20000 |
| 200 | -100 | 2000 |

For σa=200 MPa and σm=-100 MPa, applied for 2 000 cycles, we have:

- The completely reversed stress amplitude is:

Sa,r=σa1-σmσu
=2001--1001 050
=182.6 MPa

- This exceeds the endurance limit of 55.6 MPa.

- The endurance is:

NR=σar,1σarmN10.9σu≥σar≥σer∞σar<σer
=55.6182.64.27106
=6 235

- The damage is:

d4=2 0006 235
=0.321

### Total damage, repetitions and life

The total caused by one repetition of the stress spectrum over a period of 3 months, is:

D=d1+d2+d3+d4
=0.123+0+0.376+0.321
=0.82

The number of repetitions to failure is then:

Bf=1D
=10.82
=1.2

The fatigue life is:

Life=Bf×Periodrepetition
=1.2×3 months
=3.6 months

# STRESS LIFE PROBLEM

## Problem statement

300WA structural steel has the following material properties:

E = 206 GPa, fy = 300MPa,

fut =450MPa

Assume a notch fatigue factor of kf=1.7

What is the endurance limit for Psurvival=0.5?

How many cycles to failure at:

- Sa= 200MPa

- Sa= 300MPa

## Solution

Step 1: Determine the unnotched S-N curve

This is steel, and we know that the endurance ratio is given as follows:

σerb=meσut
me=0.5

For the stress at 1000 cycles, we have:

σa103=0.9σut

Step 2:  Fatigue notch factors

The fatigue notch factor at endurance was given as kf=1.7.  The figure below shows that the fatigue notch factor at 1 000 cycles is:

σut=450 MPa
=4507ksi
=64 ksi
kf'-1kf-1=0.1  From the figure below
kf'=1.07

Step 3:  Modification factors and S-N curve

The fatigue strengths at 1 000 and 1 000 000 cycles are as follows:

σer=σerb'CsizeCloadCsurfCTCrel
σerb'=σerbKf
=meσuKf
σar,103=σarb,103'CloadCTCrel
σarb,103'=0.9σuKf'

Size:

Nothing was mentioned, Csize=1.0

Load:

Cload=1, because it is assumed that the part will be subject to reversed bending.

Surface:

Nothing is said, and Csurf=1

Temperature:

Nothing is said, and CT=1.0

Reliability:

Nothing is said, and it is assumed that calculations is to be performed for 50% probability of survival.

Crel=1

S-N curve:

σarNrb=σar2N2b
σar,103103b=σer106b
σar,103 σer=103b
b=13log10σar,103 σer

# S-N CURVE STRESS LIFE EXAMPLE – same as previous problem with different S-N curve & notch fatigue factor

## Problem statement

300WA structural steel has the following material properties:

E = 206 GPa, fy = 300MPa,

fut =450MPa

Assume a notch fatigue factor of kf=1.7

What is the endurance limit Psurv=0.5?

How many cycles to failure at

- σar1 = 200MPa

- σar2 =  300MPa

## Solution

Step 1:  Define the equation for the S-N curve

In this case the yield strength is below 700 MPa, and we will assume that the S-N curve need to be modified for a notch fatigue factor at 1 000 cycles.  For the general unmodified, unnotched material, the S-N curve has the following two points:

σar1mN1=σar2mN2
σar103m103=σerm106
However, we need to modify the S-N curve for the notch by the following factors:

Kf=1+Kt-11+ar=1.7

The notch fatigue factor at 1 000 cycles, Kf' is determined as Kf'=1 as shown below.

For Sut=64 ksi, Kf'-1Kf-1=0, therefore, Kf'=1

Figure 4:  Calculation of notch fatigue factor at 1 000 cycles

The limits on the S-N curve, modified for the notch, is:

σer=0.5σutKf
=0.5×4501.7
=132 MPa
σar103=0.9σut
=405 MPa

The equation for the S-N curve is now:

NR=σerσarRmNefor σarR≥σer∞for σarR<σer

Figure 5:  S-N curve for the notched specimen

The exponent (slope), m is:

σermNe=σar103m∙103
σerσar103m=103106
mlog10σerσar103=-3
m=-3log10σerσar103
=6.18

Step 2:  Calculate endurance at requested stress amplitudes

- For σar1=200 MPa (larger than σer), the endurance is:

N1=σerσar1mNe
=1322006.18∙106
=78 090 cycles

- For σar2=300 MPa (larger than σer), the endurance is:

N2=σerσar2mNe
=1323006.18∙106
=6 382 cycles

Step 3:  General remarks

If all the stress amplitudes where endurance was required are below the endurance limit, you do not need to model the S-N curve, because, the answer is infinite life.

# S-N CURVE EXAMPLE

## Problem statement

Construct the S-N curve for a material with completely reversed stress amplitude σar1=500 MPa at Nf1=103 cycles and endurance limit σer=150 MPa at Nfe=106 cycles.  Then, calculate the endurance for the following completely reversed stress amplitudes: 300 MPa, 200 MPa, and, 100 MPa.

## Solution

The equation for the S-N curve is assumed to be: σ=ANfb.

Therefore:

A=σNfb
=σNf-b
σar1Nf1-b=σar2Nf2-b
Nf1Nf2-b=σar2σar1
b=-log10σar2σar1log10Nf1Nf2
=-0.1743

Say I need to calculate the endurance (fatigue life) at any stress amplitude, the equation becomes:

Nf1Nf2-b=σar2σar1
Nf1Nf2=σar2σar1-1b
Nfi=Nfeσerσari-1bσar103≥σari≥σer∞σari<σer

The other option is to find the equation for the S-N curve in the form σarmN=C.  For this, we use the points provided:

σar1mNf1=σar2mNf2
σar1σar2m=Nf2Nf1
m=log10Nf2Nf1log10σar1σar2

In this case, the endurance at any stress is then:

Nfi=Nfeσerσarimσar103≥σari≥σer∞σari<σer

From which it is clear that

m=-1b

# RAINFLOW COUNTING

The explanation that was done in class.

Table 2:  Rainflow counted stress spectrum over a period of 1 year

| σa | σm | Δσ | n |
| --- | --- | --- | --- |
| 45 | 35 | 90 | 0.5+0.5=1 |
| 90 | 10 | 180 | 0.5+0.5=1 |
| 25 | 25 | 50 | 0.5+0.5=1 |
| 35 | 25 | 70 | 0.5+0.5=1 |

(100;-80;180)

(80;-10;90)

(60;-10;70)

(50;0;50)

(-10;60;70)

(0;50;50)

(-80;100;180)

(-10;80;90)

Figure 1:  Stress signal over a period of 1 year

# MEAN STRESS CORRECTION

## Problem Statement

Check sensitivity for the completely reversed bending stress amplitude, σar, for the mean stress of a signal using the following mean stress correction relationships:

- Modified Goodman

- Gerber

- Smith, Watson & Topper (WST)

- Walker

Assume a material ultimate tensile strength σu=700 MPa and consider the following stress states:

| Stress amplitude [MPa] | Stress mean [MPa] |
| --- | --- |
| 100 | -100 |
| 100 | 0 |
| 100 | 100 |

## Solution

From the notes, the relevant equations are:

| Approach | Equations |
| --- | --- |
| Modified Goodman | σar=σa1-σmσu |
| Gerber | σar=σa1-σmσu2, for σm≥0 |
| SWT | σar=σmaxσa =σmax1-R2 |
| Walker | σar=σmax1-γσaγ σmax>0 =σmax1-R2γ σmax>0 γ=-0.000200σu+0.8818(σu in MPa) |

Programmed in Excel, the results are as shown in the table below.  Can you explain and make recommendations?  See your text book.

# STRESS LIFE EXAMPLE WITH MEAN STRESS CORRECTION

## Problem statement

Component undergoes cyclic stress with:

σmax = 770MPa

σmin = 70MPa

Material is steel with σu = 1,050MPa and σer = 420MPa.  The fully reversed stress at σar103 = 770 MPa.

How many cycles can be loaded on the component until fatigue crack initiation?  That is, what is the fatigue life of the component?

## Solution

### Calculate stresses and compare with endurance limit

The stress amplitude is: σa=770-702=350 MPa

The mean stress is: σm=770+702=420 MPa

Do mean stress correction.  Use Goodman:

σaσar+σmσut=1
σar=σa1-σmσut
=3501-4201050
=583 MPa
The Goodman mean stress corrected equivalent completely reversed stress amplitude is σar=583≥420 MPa, therefore, we have finite life and the S-N curve must be calculated.

### S-N curve

The S-N curve is given as:

NR=σerσarRmNefor σarR≥σer∞for σarR<σer

For which:

σar103m∙103=σerm∙106
m=log10103106log10σerσar103
=11.4

### Calculate endurance at specified stress amplitude

σar=583 MPa is larger than the endurance limit σer=420 MPa.  For this completely reversed stress amplitude, the endurance is the:

NR=σerσarRmNer
=42058311.64∙106
=23 820 cycles

# STRESS-STRAIN RELATIONSHIP

For isotropic materials we have the following stress-strain relationship:

εx=σxE-νEσy+σz
εy=σyE-νEσx+σz
εz=σzE-νE(σy+σx)

# STRAIN-LIFE EXAMPLE WITH STRAIN INPUTS

## Problem statement

The cyclic stress-strain and strain-life parameters for a steel is:

E=30 x 103 ksi; K’ = 154 ksi, σ’f = 133ksi, ε’f = 0.26, n’ = 0.202, b = -0.095,

c=-0.47

Determine the life for the histories shown on the next slide (use Morrow).

## Solution

The equations needed:

Ramberg-Osgood: ε=σE+σH'1n'

Strain-life equation: ε=σf'E2Nfb+εf'2Nfc

See the attached Excel spreadsheet.

# DAY 2: YOUR FIRST DAMAGE CALCULATION

## Problem Statement

A component undergoes axial cyclic loading as summarized in the table below, which was obtained from Rainflow cycle counting.

Table 3:  Stress spectrum for one repetition

Material is steel with Sut = 1,050 MPa with hardness 350 BHN.  The theoretical stress concentration factor at a notch on the part is Kt=2.  The notch radius is r=4 mm.  The surface finish is machined.  The shaft has a radius of 100 mm and operates at temperature T=200 °C.

How many blocks/repetitions of loading can be loaded on the component for a 1 % probability of fatigue crack initiation?  That is, what is the fatigue life of the component for a probability of survival of 99%?

## Solution

The steps that I will follow:

- Calculate notch fatigue factors:

- Calculate the influencing factors and the fatigue strength at 1 000 and 1 000 000 cycles as shown below:

Se=Se'CsizeCloadCsurfCTCrel
=0.5SutKfCsizeCloadCsurfCTCrel
S103=S103'CloadCTCrel
=0.9SutKf'CloadCTCrel

- Mean stress correction to calculate the equivalent completely reversed stress amplitude.  Use Goodman:

Sa=σa1-σmSut

- Calculate damage using the Palmgren-Miner rule

D=niNi

- Calculate the number of repetitions:

Bf=1D

- Calculate life which is (not applicable in this case):

Life=Bf×(Period of stress spectrum)

### Calculate S-N curve for the notched specimen

#### Modelling the notch effect

The theoretical stress concentration factor is Kt=2.

The ultimate tensile strength: σu=1 050 MPa.

Notch root radius: r=0.004 m=4 mm

For this we have the follow equations:

At endurance limit at 1 million cycles:

Kf=σerbun-notchedσerbnothced
Kf=1+Kt-11+αr

- Approximations for α:

α=300σuksi1.8×10-3 in.
=300×6.89σuMPa1.8×10-3×25.4 mm
=300×6.891 050MPa1.8×10-3×25.4 
=0.086 mm

Therefore:

Kf=1+2-11+0.0864
=1.98

σu=1 050 MPa=152 ksi

Fatigue notch factor at 1 000 cycles:

Kf'-1Kf-1=fσu=q

σarb,1000'=σarb,1000Kf'
σerb'=σerbKf

From the figure above, we have:

Kf'-1Kf-1=fσu=q=0.38
Kf'=0.38Kf-1+1
=0.38×0.98+1
=1.37

### Modification factors

σer=σerb'CsizeCloadCsurfCTCrel
σerb'=σerbKf
σar,103=σarb,103'CloadCTCrel
σarb,103'=0.9σuKf'

Size modification factor

The recommended modification factor for size is:

Csize=1.0, if d≤8 mm1.189d-0.097,if 8 mm<d≤250 mm

In this case, the component diameter is D=2×100=200 mm.  The modification factor for size is then:

Csize=1.189d-0.097
=1.189200-0.097
=0.71

Load modification factor

In this problem, the specimen is subject to axial loading.  The S-N curve were estimated using equations for rotating bending test.  Therefore, a modification must be made for load in this case.

σer,axial=0.70σerb

In this case, Cload=0.70.

Surface finish modification factor

From the figure below, Csurface=0.7.

Temperature modification factor

From the equation below, CT=1.0 (T=200 °C).

CT=1.0 for T≤450 ℃1-5.8-3T-450, for 450<T≤550 ℃

Reliability modification factor

From the table below, Crel=0.814.

### Mean stress correction

| Approach | Equations |
| --- | --- |
| Modified Goodman | σar=σa1-σmσu |
| Gerber | σar=σa1-σmσu2, for σm≥0 |
| Morrow | σar=σa1-σmσf' |
| SWT | σar=σmaxσa =σm+σaσa =σmax1-R2 |
| Walker | σar=σmax1-γσaγ σmax>0 =σmax1-R2γ σmax>0 γ=-0.000200σu+0.8818(σu in MPa) |

### Equation for the S-N curve

σarmN=C
σar,1mN1=σar,2mN2
m=logN2N1logσar,1σar,2
NR=σar,1σarmN10.9σu≥σar≥σer∞σar<σer

In this case, the slope of the S-N curve is calculated from the applicable fatigue strengths at 1 000 and 1 000 000 cycles as follows:

σer=σerb'CsizeCloadCsurfCTCrel
σerb'=σerbKf
σer=0.5σuKfCsizeCloadCsurfCTCrel
=0.5×10501.98×0.71×0.7×0.7×1.0×0.814
=75 MPa
σar,103=σarb,103'CloadCTCrel
σarb,103'=0.9σuKf'
σar,103=0.9σuKf'CloadCTCrel
=0.9×10501.37×0.7×1.0×0.814
=393.0 MPa

The slope of the S-N curve:

m=logN2N1logσar,1σar,2
=log 106103log393.075
=4.17

NR=75σar4.171060.9σu≥σar≥σer∞σar<σer

### Damage for one repetition

σa=100 MPa, σm=200 MPa, ni=10 000 cycles

Goodman mean stress correction:

σar=σa1-σmσu
=1001-2001050
=123.5 MPa

Endurance/fatigue life:

NR=75σar4.171060.9σu≥σar≥σer∞σar<σer
=75123.54.17106
=124 955 cycles

Damage:

di=niNi
d1=10 000124 955
=0.0800

σa=50 MPa, σm=0 MPa, ni=5 000 cycles

Goodman mean stress correction:

σar=σa1-σmσu
=501-01050
=50 MPa

Endurance/fatigue life:

NR=75σar4.171060.9σu≥σar≥σer∞σar<σer
=∞

Damage:

di=niNi
d2=5 000∞
=0

σa=100 MPa, σm=100 MPa, ni=20 000 cycles

Goodman mean stress correction:

σar=σa1-σmσu
=1001-1001050
=110.5 MPa

Endurance/fatigue life:

NR=75σar4.171060.9σu≥σar≥σer∞σar<σer
=75110.54.17106
=198 694 cycles

Damage:

di=niNi
d3=20 000198 694
=0.1007

σa=200 MPa, σm=-100 MPa, ni=2 000 cycles

Goodman mean stress correction:

σar=σa1-σmσu
=2001--1001050
=182.6 MPa

Endurance/fatigue life:

NR=75σar4.171060.9σu≥σar≥σer∞σar<σer
=75182.64.17106
=24 465 cycles

Damage:

di=niNi
d4=2 00024 465
=0.0817

#### Total damage per repetition

The total damage according to the Palmgren-Miner rule is:

D=di
=niNi
=d1+d2+d3+d4
=0.0800+0+0.1007+0.0817
=0.262

The number of repetitions to failure is then 3.8:

Bf=1D
=10.262
= 3.8

### Check with Excel

For the supplied stress spectrum, the life is 12 Blocks for a 1% probability of failure (99% probability of survival).

Table 4:  Stress spectrum for one block

### Conclusion

The fatigue life of the component for 99% probability of survival is 3.8 repetitions.

# CLASS PROBLEM

## Problem statement

The flange of a welded steel girder is classified as Detail category 125 according to BS EN 1993-1-9.  The component is subject to 500 000 cycles for stress range 200 MPa.  Adopt a safe life strategy with low consequence of failure.  The partial factor for equivalent constant amplitude stress range is γFf=1.  Is this design acceptable?.

## Solution

### Calculate the S-N curve to use

#### Partial factor for fatigue

For a safe life strategy with low consequence of failure, the partial factor for fatigue strength is γMf=1.15.

| Assessment | Consequence of failure |  |
| --- | --- | --- |
|  | Low | High |
| Damage tolerant | 1.0 | 1.15 |
| Safe life | 1.15 | 1.35 |

#### Modification factors

Size:  Nothing is said.

PWT:  Nothing said.

Corrosion:  Assume non-corrosive environment or properly surface protected.

#### Equation for the S-N curve

For this problem we use stress range with endurance in the equation as follows:

ΔσRmNR=ΔσDmNDfor 1.5fy≥ΔσR≥ΔσD, m=3ΔσDmNDfor ΔσD≤ΔσR≥ΔσL, m=5

This equation can now be changed to calculate the endurance at any stress range as follows:

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥ΔσDΔσDΔσRm2NDm2=5ΔσD>ΔσR≥ΔσL∞ΔσR<ΔσL
NC=2×106  cycles
ND=5×106  cycles
NL=100×106  cycles

ΔσC,mod=ΔσCγMfCtCTCPWT

In this case, the stress range is above the constant amplitude fatigue limit, and we have:

NR=ΔσCγMfCtCTCPWTΔσRm1NC
=1251.15∙1∙1∙120032×106 
=321 052 cycles

The endurance (or fatigue life) for 95% probability of survival is 321 052 cycles at stress range 200 MPa, which exceeds the number of cycles applied to the component, and the design complies.

# WELD FATIGUE CLASS PROBLEM

## Problem statement

## Solution

The Sr-N curve is given by the following equation:

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥ΔσDΔσDΔσRm2NDm2=5ΔσD>ΔσR≥ΔσL∞ΔσR<ΔσL
NC=2×106  cycles
ND=5×106  cycles
NL=100×106  cycles

ΔσC,mod=ΔσCγMfCtCTCPWT

### Modification factors

For damage tolerant design and high consequence of failure, the partial factor for fatigue strength is γMf=1.15.

| Assessment | Consequence of failure |  |
| --- | --- | --- |
|  | Low | High |
| Damage tolerant | 1.0 | 1.15 |
| Safe life | 1.15 | 1.35 |

The thickness modification factor is taken as Ct=1.0 in the absence of more information.

The temperature modification factor is taken as CT=1.0 in the absence of information.

No post-weld treatment is specified and CPWT=1.0.

### Calculate the points on the Sr-N curve

The modified characteristic strength is:

ΔσC,mod=361.15∙1∙1∙1
=31.1 MPa

The constant-amplitude fatigue limit is:

ΔσC,modmNC=ΔσDmND
ΔσD=ΔσC,modNCND1m  where m=3
=22.9 MPa

Are there any stress ranges exceeding the constant amplitude fatigue limit?  Yes, so we need to model the stress ranges below the constant amplitude fatigue limit.

The cut-off limit is:

ΔσLmNL=ΔσDmND
ΔσL=ΔσDNDNL1m2,  where m2=5
=22.95×10610815
=12.6 MPa

Because there are stress ranges exceeding the constant amplitude fatigue limit, the new endurance limit is the cut-off limit.

To calculate the fatigue life (endurance) for any stress range, the following applies:

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥ΔσDΔσDΔσRm2NDm2=5ΔσD>ΔσR≥ΔσL∞ΔσR<ΔσL

### Damage calculation

For Δσ=20 MPa and 1 022 000 cycles, we have:

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥22.9ΔσDΔσRm2NDm2=522.9>ΔσR≥12.6∞ΔσR<12.6
=22.92055×106
=9.84×106

The damage is: d1=1 022 0009.84×106=0.010.

For Δσ=30 MPa for 408 800 cycles, we have:

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥22.9ΔσDΔσRm2NDm2=522.9>ΔσR≥12.6∞ΔσR<12.6
=22.93035×106
=2 223 887 cycles

The damage by this stress is then: d2=408 8002 223 887=0.184

For Δσ=40 MPa for 29 200 cycles, we have:

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥22.9ΔσDΔσRm2NDm2=522.9>ΔσR≥12.6∞ΔσR<12.6
=22.94035×106
=938 203 cycles

The damage for this is then: d5=29 200938 203=0.031

The total damage is: D=d1+d2+d5=0.010+0.184+0.031=0.225.

Therefore, the total damage caused by the stress spectrum is less than 1, and the design is sufficient.

The stress spectrum can be repeated for the following number of repetitions:

Bf=1D=4.4

The fatigue life for a damage tolerant assessment with high consequence of failure is 40Bf=176 years for 95% probability of survival.

# Strain-life: Example 1

Problem statement

One repetition of the nominal stress on a Ti-6Al-4V alloy is shown in the table below.  The elastic stress concentration factor (also called the theoretical stress concentration factor) is kt=2.6.  Estimate the number of repetitions required to cause fatigue cracking at the notch.  Use the Ramberg-Osgood stress-strain relationship and the Neuber equation for notch response.

- The stress history is shown in Figure 59.

- Which was then reordered to start and end with the first peak or valley with the maximum absolute value as shown in Figure 60.

- In this case, no extrema were calculated, and exact values are used.  The stress history is short enough for this.

Figure 59:  Original stress history - 1 repetition

Figure 60:  Reordered stress history - for one repetition

Figure 61:  Stress history with stresses indicated

Solution

The material properties for Ti-6Al-4V is as follows from Dowling Table 14.1:

E=117×103 MPa
H'=1 772 MPa
n'=0.106
σf'=2030 MPa
b=-0.104
εf'=0.841 
c=-0.688

Evaluate the stress history

Rainflow counting was performed on the stress signal as shown below:

- The first step was to draw the start and stops for each reversal.

  - Note, that a few points, and one turning point could have been left out if peak-valley reduction (signal to extrema) was done before the Rainflow counting.

- Then number the peaks and valleys of the relevant cycles.  In this case the time axis will be used as was calculated in Matlab.  Otherwise use A, B, C, …. as per the examples in Dowling.

The stress-strain response is then as follows:

### Stress-strain response at the notch

The purpose of this section is to calculate the stress and strain response at the notch, and to calculate the stress and strain at every point of interest.  The points of interest are indicated in yellow in the figure below.

9

8

7

6

5

4

3

2

1

Reversal 1:  From 0 to 1, monotonic stress-strain curve

For the first stress cycle, the nominal monotonic stress amplitude is Sa=835 MPa.  The notch stress response is solved in Matlab as:

ferror=ktSa2σaE-σaE+σaH'1n'
σa1=1 192 MPa

The notch strain amplitude for the stress reversal is then:

εa=σaE+σaH'1n'
=0.0338

1:[0.0338, 1191]

Reversal 2:  1 to 2, cyclic stress strain curve

The nominal monotonic stress amplitude is Sa=835--8072=821 MPa.

Direction: ψ=-1.

The notch stress response is solved in Matlab as:

ferror=ktSa2σaE-σaE+σaH'1n'
σa1=1 186 MPa

The notch strain amplitude for the stress reversal is then:

εa=σaE+σaH'1n'
=0.0328

Therefore, the stress and strain at the end of the reversal will be:

σ2=σ1+2ψσa1

=1191+2(-1)(1186)
=-1 181 MPa
ε2=ε1+2ψεa1
=-0.0318

2:[-0.0318, -1181]

1:[0.0338, 1191]

Reversal 3:  Reversal 2 to 3, cyclic stress strain curve

3:[-0.0090, -1099]

Sa=440--8072=624 MPa
ψ=1

ferror=ktSa2σaE-σaE+σaH'1n'
σa=1 099 MPa

εa=σaE+σaH'1n'
=0.0204

σ3=σ2+2ψσa3
=1 017 MPa
ε3=ε2+2ψεa3
=-0.00902

2:[-0.0318, -1181]

1:[0.0338, 1191]

Reversal 4:  3 to 4, cyclic stress strain curve

4:[0.000845, 61]

3:[-0.0090, -1099]

Sa=440-722=184 MPa
ψ=-1

ferror=ktSa2σaE-σaE+σaH'1n'
σa=478 MPa

εa=σaE+σaH'1n'
=0.0041

σ3=σ2+2ψσa3
=61 MPa
ε3=ε2+2ψεa3
=0.000845

2:[-0.0318, -1181]

1:[0.0338, 1191]

Reversal 5:  2 to 5, cyclic stress strain curve

5:[0.02355, 1 131]

4:[0.000845, 61]

3:[-0.0090, -1099]

Sa=681--8072=745 MPa
ψ=1

ferror=ktSa2σaE-σaE+σaH'1n'
σa=1 156 MPa

εa=σaE+σaH'1n'
=0.0277

σ5=σ2+2ψσa5
=1 131 MPa
ε5=ε2+2ψεa5
=0.02355

2:[-0.0318, -1181]

1:[0.0338, 1191]

Reversal 6:  5 to 6, cyclic stress strain curve

6:[-0.00927, -975]

5:[0.02355, 1 131]

4:[0.000845, 61]

3:[-0.0090, -1099]

Sa=681--4122=547 MPa
ψ=-1

ferror=ktSa2σaE-σaE+σaH'1n'
σa=1 053 MPa

εa=σaE+σaH'1n'
=0.0164

σ6=σ5+2ψσa6
=-975 MPa
ε6=ε5+2ψεa6
=-0.00927

2:[-0.0318, -1181]

1:[0.0338, 1191]

Reversal 7:  6 to 7, cyclic stress strain curve

7:[0.00722, 723]

6:[-0.00927, -975]

5:[0.02355, 1 131]

4:[0.000845, 61]

3:[-0.0090, -1099]

Sa=283--4122=348 MPa
ψ=1

ferror=ktSa2σaE-σaE+σaH'1n'
σa=849 MPa

εa=σaE+σaH'1n'
=0.00822

σ5=σ2+2ψσa5
=723 MPa
ε5=ε2+2ψεa5
=0.00722

2:[-0.0318, -1181]

1:[0.0338, 1191]

Reversal 8:  7 to 8, cyclic stress strain curve

8:[0.00477, 437]

7:[0.00722, 723]

6:[-0.00927, -975]

5:[0.02355, 1 131]

4:[0.000845, 61]

3:[-0.0090, -1099]

Sa=283-1732=55 MPa
ψ=-1

ferror=ktSa2σaE-σaE+σaH'1n'
σa=143 MPa

εa=σaE+σaH'1n'
=0.00122

σ8=σ7+2ψσa8
=437 MPa
ε8=ε7+2ψεa8
=0.00477

2:[-0.0318, -1181]

1:[0.0338, 1191]

Reversal 9:  2 to 9, cyclic stress strain curve

9:[0.0338, 1 191]

8:[0.00477, 437]

7:[0.00722, 723]

6:[-0.00927, -975]

5:[0.02355, 1 131]

4:[0.000845, 61]

3:[-0.0090, -1099]

Sa=835--8072=821 MPa
ψ=1

ferror=ktSa2σaE-σaE+σaH'1n'
σa=1 186 MPa

εa=σaE+σaH'1n'
=0.0328

σ9=σ2+2ψσa9
=1 191 MPa
ε9=ε2+2ψεa9
=0.0338

2:[-0.0318, -1181]

1:[0.0338, 1191]

### Matlab commands: notch stress and strain at every point

Filename: strain_life_classproblem_2020_04_23.mlx

Class problem in strain-life

Date: 2020-04-23 done during class time.

E=117e3;

Ha=1772;na=0.106;sigfa=2030;b=-0.104;

epsfa=0.841;c=-0.688;

kt=2.6;

ferror=@(Sa,kt,E,sa,Ha,na) (kt*Sa)^2./sa/E-(sa/E+(sa/Ha).^(1/na));

epsa=@(sa,E,Ha,na) sa/E+(sa./Ha).^(1/na);

% Cycle 1: 0 to 835 MPa, Monotonic

Sa=835;sa=fzero(@(sa) ferror(Sa,kt,E,sa,Ha,na),[1 2000]);

psi=1

sa1=sa

epsa1=epsa(sa,E,Ha,na)

s1=0+psi*sa1

eps1=0+psi*epsa1

% Cycle 2: 835 to -807

Sa=(835--807)/2;sa=fzero(@(sa) ferror(Sa,kt,E,sa,Ha,na),[1 2000]);

psi=-1

sa2=sa

epsa2=epsa(sa,E,Ha,na)

s2=s1+psi*2*sa2

eps2=eps1+psi*2*epsa2

% Cycle

Sa=(440--807)/2,sa=fzero(@(sa) ferror(Sa,kt,E,sa,Ha,na),[1 2000]);

psi=1

sa3=sa

epsa3=epsa(sa,E,Ha,na)

s3=s2+psi*2*sa3

eps3=eps2+psi*2*epsa3

Sa=(440-72)/2,sa=fzero(@(sa) ferror(Sa,kt,E,sa,Ha,na),[1 2000]);

psi=-1

sa4=sa

epsa4=epsa(sa,E,Ha,na)

s4=s3+psi*2*sa4

eps4=eps3+psi*2*epsa4

Sa=(682--807)/2,sa=fzero(@(sa) ferror(Sa,kt,E,sa,Ha,na),[1 2000]);

psi=1

sa5=sa

epsa5=epsa(sa,E,Ha,na)

s5=s2+psi*2*sa5

eps5=eps2+psi*2*epsa5

Sa=(681--412)/2,sa=fzero(@(sa) ferror(Sa,kt,E,sa,Ha,na),[1 2000]);

psi=-1

sa6=sa

epsa6=epsa(sa,E,Ha,na)

s6=s5+psi*2*sa6

eps6=eps5+psi*2*epsa6

Sa=(283--412)/2,sa=fzero(@(sa) ferror(Sa,kt,E,sa,Ha,na),[1 2000]);

psi=1

sa7=sa

epsa7=epsa(sa,E,Ha,na)

s7=s6+psi*2*sa7

eps7=eps6+psi*2*epsa7

Sa=(283-173)/2,sa=fzero(@(sa) ferror(Sa,kt,E,sa,Ha,na),[1 2000]);

psi=-1

sa8=sa

epsa8=epsa(sa,E,Ha,na)

s8=s7+psi*2*sa8

eps8=eps7+psi*2*epsa8

Sa=(835--807)/2,sa=fzero(@(sa) ferror(Sa,kt,E,sa,Ha,na),[1 2000]);

psi=1

sa9=sa

epsa9=epsa(sa,E,Ha,na)

s9=s2+psi*2*sa9

eps9=eps2+psi*2*epsa9

### Fatigue

From the figure below, the nominal stress cycles with number of cycles are as follows:

| From | To | Number of cycles ni |
| --- | --- | --- |
| 0 | 1 | 1 |
| 1 | 2 | 1 |
| 3 | 4 | 1 |
| 5 | 6 | 1 |
| 7 | 8 | 1 |

9

8

7

6

5

4

3

2

1

The steps to calculate the mean stress compensated fatigue life at the notch is as follows:

STEP 1:  The zero-mean-stress-equivalent fatigue life is given by:

εa=σf'E2N*b+εf'2N*c
ktSa2σaE=σf'E2N*b+εf'2N*c
ferrsl=σf'E2N*b+εf'2N*c-ktSa2σaE

STEP 2:  The mean-stress compensated fatigue life is:

Nf=Nmi*1-σmσf'-1b

This was programmed in the excel sheet on the next page.

The filename of the Excel Workbook is: Strainlife.xls

The use of the solver was demonstrated in class, as well as the use of Matlab to find the damage.

# WELD FATIGUE EXAMPLE PROBLEM 2020-06-11

## Problem statement

Note, to obtain maximum points for each problem clearly motivate solutions and equations used.

The H-beams shown below are joined by a complete joint penetration butt weld (made from both sides) with no cope holes.  The web and flange thickness are 45 mm.  The height of the weld convexity is less than 10% of the weld width with smooth transition to the plate surface.  Weld run-on and run-off pieces were used during welding and removed.  The edges were then ground flush in the direction of the stress.  An NDT inspection revealed no defects in the weld.  The operating temperature is 400 ℃ and the surface is not protected.  The steel beam is used in an environment where pit corrosion is likely.  No stress-relieving was done, and the stress spectrum shown below was determined without reducing the compression parts of the signal to 60% of its value as would be the case to make provision for stress-relieving.

Questions

- What is the fatigue life of the component, in years, for 95% probability of survival, for the load spectrum given below?  Assume a low consequence of failure and damage tolerant design.

- Will this detail category benefit from weld toe dressing?

Table 1:  Stress spectrum for a period of 10 days

Figure 1:  H-beam under axial loading

## Solution

### Detail category

From the standard, it was determined that this welded joint falls under detail category 90 (as shown below), and, for this detail category thickness modification shall be included.

### Modification factors

Detail category was 90, which means, a strength of 90 MPa range at 2 000 000 cycles.

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥ΔσDΔσDΔσRm2NDm2=5ΔσD>ΔσR≥ΔσL∞ΔσR<ΔσL
NC=2×106  cycles
ND=5×106  cycles
NL=100×106  cycles

ΔσC,mod=0.7ΔσCγMfCtCTCPWT, cut-off limit not applicable

#### Partial factor for fatigue strength

For the damage tolerant design and low consequence of failure, the partial factor for fatigue strength is γMf=1.0.

| Assessment | Consequence of failure |  |
| --- | --- | --- |
|  | Low | High |
| Damage tolerant | 1.0 | 1.15 |
| Safe life | 1.15 | 1.35 |

#### Thickness

The detail category requires thickness to be considered when exceeding 25 mm as follows (for the flange thickness of 45 mm:

Ct=ks=1for t≤2525t0.2for t≥25
=25450.2
=0.89

#### Temperature

The component is used at a temperature of 400 ℃, for which the temperature modification factor is CT≈0.72 from the figure below.

#### Post-weld treatment

No post-weld treatment is specified and CT=1.0.

### Constant amplitude fatigue limit

The constant amplitude fatigue limit is as follows:

0.7ΔσcCtCTCPWTγMf32×106=ΔσD3×5×106
ΔσD=0.7ΔσcCtCTCPWTγMf2×1065×106m1
=29.7 MPa

Are there any stress ranges exceeding the constant amplitude fatigue limit?  Yes.  But, in this case, even if all stress ranges were below the constant amplitude fatigue limit, we should still do damage calculation because we operate in a corrosive environment in which the fatigue limit is not applicable.  This is also the reason why in this case the part of the Sr-N curve with slope m2=5, does not stop at the cut-off limit.

### Sr-N curve

The equation for the Sr-N curve now becomes:

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥ΔσDΔσDΔσRm2NDm2=5ΔσD>ΔσR
ΔσD=29.7 MPa

### Damage

For Δσ=90 MPa for 200 cycles, we have

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥ΔσDΔσDΔσRm2NDm2=5ΔσD>ΔσR
=29.79035×106
=179 685 cycles
ΔσD=29.7 MPa

The damage is: d90=200179685=1.11×10-3

For Δσ=45 MPa for 2 000 cycles, we have

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥ΔσDΔσDΔσRm2NDm2=5ΔσD>ΔσR
=29.74535×106
=1 437 480 cycles
ΔσD=29.7 MPa

The damage is: d45=2 0001 437 480=1.39×10-3

For Δσ=15 MPa for 2 000 000 cycles, we have

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥ΔσDΔσDΔσRm2NDm2=5ΔσD>ΔσR
=29.71555×106
=152 158 408 cycles
ΔσD=29.7 MPa

The damage is: d15=2 000 000152 158 408=1.31×10-2

This damage must be taken, even though the cut-off limit can be calculated at 100 million cycles.  15 MPa stress range is below the cut-off limit.  If the component was not in a corrosive environment, or, if proper surface protection was implemented, the endurance would have been infinite for 15 MPa stress range.

The total damage caused by the stress spectrum is:

D=d90+d45+d15
=1.56×10-2

The number of repetitions of the stress spectrum is:

Bf=1D=11.56×10-2=63.9

The fatigue life, in years, for 95% probability of survival, is then:

Life=Period×Bf=PeriodD=10365×63.9=1.75 years

### PWT: Weld toe dressing

According to the standard, the benefit of toe dressing is as follows:

Grinding & TIG dressing:

Effective stress range: Δσ=Δσ

Steel:

ΔσC=min1.3×ΔσC112

Aluminium:

ΔσC=min1.3×ΔσC45

But, in this case the surface is exposed to a corrosive environment, in which case dressing will not benefit the life.  Therefore, the surface must be protected, in which case the detail category will be:

ΔσC×90=117, but this is larger than 112
Therefore:
ΔσC=112 MPa

# FRACTURE CONTROL PLAN

Time, N, rotations, etc

Crack size, a, [mm]

Now

# WELD FATIGUE

## Problem statement

Note, to obtain maximum points for each problem clearly motivate solutions and equations used.

The H-beams shown below are joined by a complete joint penetration butt weld (made from both sides) with no cope holes.  The web and flange thickness is 45 mm.  The height of the weld convexity is less than 10% of the weld width with smooth transition to the plate surface.  Weld run-on and run-off pieces were used during welding and removed.  The edges were then ground flush in the direction of the stress.  An NDT inspection revealed no defects in the weld.

Questions

- What is the fatigue life of the component, in years, for the load spectrum given below?  Assume a low consequence of failure and damage tolerant design.

- Will this detail category benefit from weld toe dressing?

Table 1:  Stress spectrum for a period of 10 days

Figure 1:  H-beam under axial loading

# CLASS PROBLEM ON 2020-05-22

The flange of a welded steel girder is classified as Detail category 125 according to BS EN 1993-1-9.  The component is subject to 500 000 cycles for stress range 200 MPa.  Adopt a safe life strategy with low consequence of failure.  The partial factor for equivalent constant amplitude stress range is ﷐𝛾﷮𝐹𝑓﷯=1.0.  Is this design acceptable?

## Solution

The problem indicates a safe life assessment method with low consequence of failure.  Therefore, the partial factor for fatigue is γMf=1.15.

| Assessment method | Consequence of failure |  |
| --- | --- | --- |
|  | Low consequence | High consequence |
| Damage tolerant | 1.00 | 1.15 |
| Safe life | 1.15 | 1.35 |
| Source: BS EN 1993-1-9, 2005:11 |  |  |

The approach is as given in the table below.  The equation for the Sr-N curve is:

ΔσR1mNR1=ΔσRimNRi
m1=3
m2=m1+2=5

ΔσCγMf

ΔσD=ΔσCγMf2 000 0005 000 0001m1=80 MPa

ΔσL=ΔσD5 000 000100 000 0001m2=44 MPa

Check 1:  Calculate the endurance at stress range 200 MPa and compare with the required fatigue life

ΔσR1mNR1=ΔσRimNRi
m1=3
m2=m1+2=5
NR=ΔσCγMf200m1NC,  NC=2×106 cycles
=321 052 cycles

The endurance is less than the required fatigue life of 500 000 cycles, and the design does not comply.

Check 2: Calculate the stress range from the fatigue curve at 500 000 cycles, and compare against the applied stress range of 200 MPa.

ΔσR1mNR1=ΔσRimNRi
m1=3
m2=m1+2=5
ΔσR1=ΔσCγMf∙2 000 000500 0001m1
=172 MPa

The fatigue strength at 500 000 cycles is 172 MPa stress range, which is less than the applied stress range of 200 MPa, and, the design does not comply.

# LINKSPAN WELD FATIGUE DESIGN

The fatigue performance of a welded detail in a steel linkspan structure can be represented by a fatigue curve corresponding to BS EN 1993-1-9 Detail Category 36.  The linkspan carries typical vehicles of weight 1, 2 and 5 ton.  A linear elastic finite beam element analysis revealed the stress ranges in the welded detail as summarised in the table on the right with the proportion of vehicles carried by the ferry 70%, 28% and 2% respectively as summarised in the table.  The linkspan is used twice per day.  No more than one vehicle can occupy the linkspan at any one time.  The design life required is equal to the service life of 40 years.  Is this design sufficient if a damage tolerant with high consequence of failure strategy is implemented?  A total of 50 vehicles are carried per day, and two stress cycles are caused to the linkspan per vehicle (on- and off loading).  The part is corrosion protected and the operating temperature is 300 °C.

Check:

1 ton vehicles

n=40∙365∙50∙2∙70%

=1 022 000

Add the following to the stress spectrum:

Δσ,n:(15 MPa, 3 000 000) and (7 MPa, 100 000 000)

Solution

The equation for the Sr-N curve for large scale manufactured components:

ΔσC,mod=ΔσCγMfCtCTCPWT
ΔσD=ΔσC,modNCND1m1

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥ΔσDΔσDΔσRm2NDm2=5ΔσD>ΔσR≥ΔσL∞ΔσR<ΔσL
NC=2×106  cycles
ND=5×106  cycles
NL=100×106  cycles

ΔσC,mod=ΔσCγMfCtCTCPWT

### Partial factor for fatigue

In this case γMf= 1.15.

| Assessment method | Consequence of failure |  |
| --- | --- | --- |
|  | Low consequence | High consequence |
| Damage tolerant | 1.00 | 1.15 |
| Safe life | 1.15 | 1.35 |
| Source: BS EN 1993-1-9, 2005:11 |  |  |

### Thickness modification

Nothing is said about thickness, so Ct=1.0.

### Temperature modification

At 300 ℃ CT=0.85.

### Post-weld treatment

Nothing is mentioned, take CPWT=1,0.

ΔσC,mod=ΔσCγMfCtCTCPWT
=361.15∙1.0∙0.85∙1.0
=26.7 MPa
NC=2×106 cycles

ΔσD=ΔσC,modNCND1m1, ND=5E6;m1=3
=26.72513
=19.6 MPa

ΔσL=ΔσDNDNL1m2, NL=100E6;m2=5
=19.65100 15
=10.8 MPa

### Damage and fatigue

The equation from which the endurance at any stress range can be calculated is as follows:

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥ΔσDΔσDΔσRm2NDm2=5ΔσD>ΔσR≥ΔσL∞ΔσR<ΔσL

For ΔσR=20 MPa applied for 1 022 000 cycles we have:

NR20=19.6203∙5×106=4 709 890 cycles
d20=1 022 0004 709 890=0.217

For Δσ30=30 MPa applied for 408 800 cycles we have:

NR30=NR20=19.6303∙5×106=1 395 522 cycles
d30=408 8001 395 522=0.293

For Δσ40=40 MPa and 29 200 cycles we have:

NR40=19.6403∙5×106=588 736 cycles
d40=29 200588 736=0.050

For Δσ15=15 MPa and 3 000 000 cycles we have:

NR15=19.6155∙5×106=19 045 573 cycles
d15=3 000 00019 045 573=0.156

For Δσ7=7 MPa and 100 000 000 cycles we have:

NR7=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥ΔσDΔσDΔσRm2NDm2=5ΔσD>ΔσR≥ΔσL∞ΔσR<ΔσL
=∞
d7=0

The total damage is:

D=d20+d30+d40+d15+d7
=0.217+0.293+0.050+0.158+0
=0.718

Repetitions to failure:

Bf=1D=1.4

The fatigue life:

L=Period×Bf
=40×1.4
=56 years

Therefore, the design is OK.

# WELD FATIGE CLASS PROBLEM INCLUDING ALL

An 8 mm double fillet weld was used in a T-joint as shown below.  The stress spectrum was calculated over a period of 5 years and is summarized in the table below.  The surface is corrosion protected.  The component operating temperature is at 250 °C.  Because of the small weld that was used in the construction, the weld toes were burred to specification, and peened to specification afterwards.  The stress range has in all cases a stress ratio of R=-0.2.  The component was heat treated before post-weld treatment.  The design strategy is damage tolerant with low consequence of failure.  What is the fatigue life of the component?

Table 5:  Stress spectrum over a period of 5 years

Δσ

50

50

Width: w=200

## Solution

The following procedure will be used:

- Find the partial factor for fatigue.

- Calculate modification factors:

  - Temperature.

  - Size.

  - Post-weld treatment.

  - Heat-treatment effects.

- Determine detail categories.

- Determine the equation for the S-N curve for crack initiation at the:

  - Weld toe.

  - Weld root.

- Calculate damage.

- Calculate life.

### Partial factor for fatigue

For a damage tolerant and low consequence of failure, the partial factor for fatigue is γMf=1.0.

### Modification factors/effects

#### Temperature

The modification factor for operation at 250 °C is CT=0.9.

### Detail category: crack initiation at the weld toe

The detail category for crack initiation at the weld toe is ΔσCtoe=71.  This detail will benefit from heat treatment, weld toe treatment, and, peening.

### Detail category: crack initiation in the weld root

In this case, the detail category is marked with an *, and can be moved one category up.  In this case conservativeness is not so important and the detail category was raised by one level to ΔσCthroat=40 (see S-N curves below).  This detail will NOT benefit from weld toe treatment or peening.  But, it will benefit from heat treatment.

### Heat treatment

In this case heat treatment allows the use of 60% of the compressive part in the stress signal for range calculation.  The stress spectrum only provides the stress range and stress ratio.  To calculate the compressive stress and effective stress range for every given stress range, the following equation was used:

R=σminσmax
RHT=0.6σminσmax=0.6R
σmin=Rσmax
Δσ=σmax-σmin
=σmax(1-R)

Steps to follow:

- Calculate σmax=Δσ1-R

- Calculate new stress range from: ΔσHT=σmax1-RHT=Δσ×1-RHT1-R

### Grinding and peening for improvement at the weld toe

The problem statement mentioned grinding, then peening afterwards.  In this case, we can have the benefit of both provided that we do not exceed the limits as specified.

#### Grinding

For toe grinding the benefit and finale characteristic strength is:

ΔσCg=min1.3ΔσC112

#### Peening

The benefit from peening after grinding is:

ΔσCp=min1.3ΔσCg112

### Stress in the weld throat

The stress in the weld throat from the nominal stress as given will be calculated as follows:

Δσwaww=Δσtw
Δσw=Δσtaw

### Damage calculation and fatigue life assessment

The equation for the S-N curve will calculated endurance for any stress range as follows:

NR=ΔσDΔσRm1NDfor ΔσD≤ΔσR≤1.5fy, m1=3ΔσDΔσRm2NDfor ΔσL≤ΔσR<ΔσD, m2=5 ∞for ΔσR<ΔσL

### Fatigue life for crack initiation at the weld toe

The fatigue life for 95% probability of survival for crack initiation at the weld toe is 16.9 years.

### Fatigue life for crack initiation at the weld throat

The fatigue life for 5% probability of crack initiation in the weld throat is 2.16 days!  Please redesign this thing.

# THIN WALL PRESSURE CYLINDER

The force that holds the longitudinal loads:

Cross-section area of steel: A=πDt
Area of pressure force: FP=π4D2P
Stress produced in steel:

σA=Fp=π4D2P
σ=π4D2πDtP
=DP4t

# PRESSURE VESSEL DESIGN EXAMPLE

## Problem statement

## Solution

### Material selection

Choose plate steel to SA 2062.  Line 23 below.

The allowable stress at the operating temperature, assume room temperature, is: S=117 MPa.

### Joint efficiency

Assume no radiography.  Assume welds are all butt welds according to the description below, from which the joint efficiency is E=0.7.

### Thickness to use in calculation of design pressure

The thickness of 25.4 mm plate, specified by the client, includes a corrosion allowance of 3.2 mm.  Therefore, the thickness to use in determining the design pressure shall be 25.4-3.2=22.2 mm

### Maximum allowable operating pressure

We know that the longitudinal (Category A) welds are loaded to the highest stress.  Or, in other words, the circumferential stress will govern the maximum allowable pressure.

The maximum allowable operating pressure:

P=SE1tr+0.6t
=117×0.7×22.2(500+3.2)+0.6×22.2
=3.5 MPa

# Acceptable fatigue design question

## Problem Statement

The flange of a welded steel girder is classified as Detail category 125 according to BS EN 1993-1-9.  The component is subject to 500 000 cycles for stress range 200 MPa.  Adopt a safe life strategy with low consequence of failure.  The partial factor for equivalent constant amplitude stress range is γFf=1.0.  Is this design acceptable?

## Solution

Partial factor for fatigue:

From the table below, the partial factor for fatigue strength for safe life and low consequence of failure is γMf=1.15.

Modification factors

No modification effects requested.  So, none applicable.

Fatigue curve

For the stress range given above, the S-N curve equations can be manipulated as below to calculate the endurance at any stress range:

NR=ΔσcγMfΔσR 3Nc=1251.1520032×106=321 000 cycles.  Therefore, the endurance at 200 MPa is 321 000 cycles, which is below the  required 500 000 cycles, and, the design do not comply.

ALTERNATIVELY

ΔσC=125 MPa

Steps:

- Calculate the stress range at 500 000 cycles, for the partial factor for fatigue modified Sr-N curve.

- Check if the applied stress range is below the stress range calculated above, if so, the design is acceptable.

Could also:

- Calculate the endurance at stress range 200 MPa from the partial factor modified Sr-N curve.

- If the applied number of cycles is < than this endurance, the design is acceptable.

Modification factors

In this case we only need to modify for the safe life strategy with high consequence of failure, for which γMf=1.15.

### Check 1

The stress range that the Sr-N curve allows at endurance 500 000 cycles is:

ΔσR=ΔσCγMf∙NCNR1m1

Assume the slope of the Sr-N curve is m1=3.

Therefore:

ΔσR=1251.152×10650000013
=172 MPa

This stress range is BELOW the applied stress range, and the design is not acceptable.

### Check 2: Calculate endurance

The endurance NR at 200 MPa stress range is 321 000 cycles, which is less than the required 500 000 cycles and the design is not acceptable:

NR=ΔσCγMfΔσRm1NC
=1251.152003×2×106
=321 000 cycles

# WELD FATIGE EXAMPLE ON 2017-08-15

## Problem statement

The fatigue performance of a welded detail in a steel linkspan structure can be represented by a fatigue curve corresponding to BS EN 1993-1-9 Detail Category 36.  The linkspan carries typical vehicles of weight 1, 2 and 5 ton.  A linear elastic finite beam element analysis revealed the stress ranges in the welded detail as summarised in the table on the right with the proportion of vehicles carried by the ferry 70%, 28% and 2% respectively as summarised in the table.  The linkspan is used twice per day.  No more than one vehicle can occupy the linkspan at any one time.  The design life required is equal to the service life of 40 years.  Is this design sufficient if a damage tolerant with high consequence of failure strategy is implemented?  A total of 50 vehicles are carried per day, and two stress cycles are caused to the linkspan per vehicle (on- and off loading).

The exhaust pipe blows are at temperature 350 °C on the link.  No post-weld treatment was done, as it was reserved for when failures occur.

## Solution

### Steps

The following steps will confirm the design:

- Calculate the partial factor for fatigue.

- Calculate temperature modification factor.

- Calculate total damage and fatigue life.

### Partial factor for fatigue

For a damager tolerant and high consequence of failure strategy, the partial factor for fatigue is γMf=1.15.

### Temperature modification factor

The modification factor for temperature for operating at 350°C is CT=0.79.

CT350°C=0.79

### Equation for the S-N curve

The endurance is given as follows:

NR=Δσc'ΔσRm1Ncfor ΔσD≤ΔσR≤1.5fyΔσDΔσRm2NDfor ΔσL≤ΔσR≤ΔσD∞for ΔσR≤ΔσL

The important points on the S-N curve is then:

ΔσD=ΔσcγMf×CT NcND13=18.2 MPa
ΔσL=ΔσDNDNL15=10 MPa

### Damage calculation

For 20 MPa:

NR=ΔσDΔσRm1ND=18.22035×106=3 781 248

D20=1 022 0003 781 248=0.27

For 40 MPa:

NR=470 981
D40=0.87

For 100 MPa:

NR=30 249
D100=0.97

The total damage is then:

The total damage is then:

DT=D20+D40+D100
=2.11

Therefore the design life of the link for the specified stress spectrum is:

DesLife=402.11
=20 years

### The stress spectrum

To calculate the applied cycles over the design life of 40 years, the following formula was used:

ni=50×2×365×40×Pi

## Steps

- Construct the Sr-N cure.  Modify for

  - Partial fatigue strength factor, γMf.

  - Temperature.

  - Post-weld treatment.

- Calculate damage.

- Calculate life.

- Make recommendations on the use of post—weld treatments if the fatigue life is < design life required.

## Calculate damage

The equation of the Sr-N curve that will be used to calculate endurance, is as follows:

NR=ΔσC,modΔσRm1NC for ΔσD≤ΔσR<1.5SyΔσDΔσRm2NDfor ΔσL≤ΔσR<ΔσD∞for ΔσR<ΔσL

## What about post-weld treatment

The first to verify, is if the post-weld treatment will be of any benefit for the detail.

When we do peening.

- Special requirements

  - Maximum of nominal compressive stress including proof loading <0.25fy

    - Assume we comply

  - Dependent on stress ratio:

    - R<0 effective stress range = Δσ

    - 0<R≤0.4 effective stress range = maximum applied stress σ

    - R>0.4 no benefit

It is assumed that the link is only loaded on one direction, from zero stress to a maximum value equal to the range.  In this case R=0.  Therefore, the effective stress range is as given in the table.

Assume the material is structural steel 350W.  For this material, the benefit from peening is as follows:

Benefit=1.3ΔσC with maximum 112 MPa

# PRESSURE VESSEL EXAMPLE 2020-06-12

## Problem Statement

- A fabricator of a pressure vessel elected to use as 25.4 mm plate made of:

  - Specify the material

- The radius should be 500 mm

- Determine the allowable working pressure of the cylindrical section of the pressure vessel

- Corrosion Allowance:

  - Make provision for 3.2 mm for corrosion

- The operating temperature is 600 ℉.

Answer in class in the class notes document

## Solution

Procedure to follow:

- Select material.

  - ASME Section II, Part D.

  - From this, I will obtain the maximum allowable design stress.

- Joint efficiency.

- Reduce plate thickness with corrosion allowance.

- Calculate allowable working pressure.

### Material selection

From the table below, I recommend the use of SA 537 plate.  See Line 16.

The material properties:

From the figure below, the minimum ultimate tensile and yield strengths are 70 and 50 ksi respectively.

From the figure below the figure below, the maximum allowable design stress at 600 ℉ is 19.5 ksi.

From the table below, the maximum allowable pressure is given as:

P=SEtr+0.6t

In this case, to make provision for corrosion, the internal radius and thickness are:

r=0.5+0.0032
=0.5032 m

The thickness to use in this case is:

t=25.4-3.2
=22.2 mm

#### Joint efficiency

The problem statement does not indicate any radiographic post-weld inspections and the vessel will be designed to make provision for no radiographic inspection.  No detail was provided on the make-up of the joints.

For this case and for Category A, the joint efficiency is E=0.65.

#### Maximum allowable pressure

Therefore, the maximum allowable pressure in this pressure vessel is:

P=SEtr+0.6t
=19.5×6.89×0.65×22.2503.2+0.6×22.2
=3.75 MPa

# PRESSURE VESSEL AND CHECK FOR BUCKLING

## Problem statement

- A horizontal vessel with inside diameter 1,500 mm is to be fabricated from SA-516 Grade 70 material.  The design pressure at the top of the vessel is 3,378 kPa (3.4 MPa) at 216 °C.   This measurement point was at a height of 1.5 m above the centerline of the cylinder.

  - All longitudinal joints shall be Type 1 and spot radiographed in accordance with UW-52

  - Circumferential joints are Type 1 with no radiography

- Vessel operates full of liquid with density 998 kg/m3.  Distance from the centerline to the uppermost part of vessel is 1.5 m.

- Determine the required thickness at Point A

  - Neglect the weight of the vessel in the calculation

- UG-22 states that the static head of the liquid must be included in the pressure P

## Solution

- Calculate the design pressure.

- Find the maximum allowable design stress.

- Circumferential stress

  - Find joint efficiency.

  - Calculate t

- Longitudinal stress at the bottom

  - Find joint efficiency

  - Calculate bending stress

  - Calculate t

  - Calculate stress at the top of the vessel.

    - If < 0, check for buckling.

- Add thickness for corrosion

### Design pressure

The pressure at the top of the vessel was given 3 378 kPa.  However, hydrostatic pressure need to be included and from this the design pressure is:

P=3 378×103+ρgh
=3 378×103+998×9.81×2.25
=3.4 MPa

### Maximum allowable design stress

The temperature is 443 °F.  For this, the maximum allowable stress is 20 ksi, 140 MPa.

### Circumferential stress

#### Joint efficiency and thickness

The joint efficiency for the longitudinal welds is E=0.85.  The thickness required is:

t=PrSE-0.6P
=3400×0.75140000×0.85-0.6×3400
=21.8 mm

Confirm that this thickness is available for the material.

### Longitudinal stress at the top

The longitudinal stress due to pressure and bending is given by the following equation:

σtop=MyI+PR+0.2tt
=-WL2Ro8∙π4Ro4-Ri4+PRi+0.2tt

=-3.4 MPa  Ag nee, this is tto small to demonstrate buckling.  Say it is:
=-80 MPa

The maximum bending moment is at the centre of the pressure vessel:

M=WL28
W=9.81×998πr2
L=303.3=9 m

P=2SEtR+0.2t
SE=PR+0.2tt

There is compressive stress.  Confirm buckling.

### Confirm buckling

Step 1:  Calculate A

A=0.125Rot
=0.0034

Step 2:  Factor B from graph

From the graph below, the factor is B=12.400 ksi ~100 MPa.  Therefore, the thickness is adequate to prevent buckling because B=100 MPa is more than the compressive stress of 80 MPa.

### Check longitudinal stress at bottom

σb=WL2Ro8∙π4Ro4-Ri4
=3.6 MPa

This is small contribution and will be neglected.

# PLANE STRESS AND STRAIN

The constitutive model for isotropic materials:

εx=σxE-νEσz+σy
εy=σyE-νEσz+σx
εz=σzE-νEσx+σy

Say we have stress state: σx=1, σy=0 and σz=0

Under plane strain conditions, the strains εy=ε-z=0.  Then stresses σy and σz will be generated because:

εx=σxE-νEσz+σy
0=σyE-νEσz+σx
0=σzE-νEσx+σy

# FRACTURE MECHANICS

# FRACTURE MECHANICS CLASS PROBLEM

## Problem statement

You have a rectangular cross section steel part with yield strength 500 MPa and Charpy test energy 35 J that has a double edge crack measured 2 mm on each side.  The part is subject to an axial stress amplitude 100 MPa, mean 0 MPa, for 50 cycles per hour.  The width of the part is 250 mm and thickness 30 mm.  The part is used for 8 hours per day.  For how long can the part be used before failure?  What can be done to increase the fatigue life?

## Solution

Steps:

- Determine the plane strain fracture toughness of the material.

- Calculate the crack size where failure occur.

  - Fracture

  - Plastic collapse

- Get a model for the geometric stress concentration factor.

- Set up the Paris rule for crack propagation.

- Solve

### Plane strain fracture toughness

A lower bound for the plane strain fracture toughness will be used, given by:

KIc=21.6Cv0.17  MPam

### Fracture

Fracture occurs when the crack size reaches a value so that the stress intensity factor equals the plane strain fracture toughness at the maximum tensile stress:

KI=βaσπa
afr=1πKICβafrσmax2

The geometric stress concentration factor is given by the following figure:

### Plastic collapse

Plastic collapse occurs when the crack size reaches a value so that the stress in the remaining section becomes equal to the yield strength:

σrem=FnomBW-2a
=σnomWBBW-2a
SyW-2acol=σnomWBB
W-2acol=σnomWBBSy
2acol=W-σnomWBBSy
acol=12W-σnomWBBSy

### Crack propagation

The crack propagation will be modelled as follows:

dadN=CΔK+m
where

C=1×10-8
m=3

## Calculation sheet

For this load application the stress ration is -1.  Therefore the threshold stress intensity level is 5.4 MPam0.5.  The applied stress intensity range is 8.9 MPam0.5, which is higher than threshold value, and, crack propagation will occur.  From the table below, the crack will propagate to 36 mm in 450 cycles where the fracture toughness is reached.  The component fails in fracture.  For fracture collapse, a material with plane strain facture toughness of 70 MPam0.5 or more is required to allow the crack to grow to 100 mm in length.

Life can be extended by:

- Repairing the crack.

- Drill-stop the crack.

- Retard the crack by tensile overloading.