# FORMULA SHEET: Fatigue, Fracture Mechanics

## Structural Mechanics

σi=MxyiIxx-MyxiIyy+FA
εx=σxE-νEσy+σz+αΔT

## Fatigue: Machined Components

σarmN=C
σar,1mN1=σar,2mN2
m=logN2N1logσar,1σar,2
NR=σar,1σarmN10.9σu≥σar≥σer∞σar<σer

OR

σarNb=C
σar,1N1b=σar,2N2b
b=logσar,1σar,2logN2N1
NR=σar,1σar1bN10.9fut≥σar≥Se∞σar<Se

Endurance limit estimates (see Dowling Table 10.1)

σerb=0.25BHN ksifor BHN≤400100 ksifor BHN>400

Steel

σerb=0.5σufor σu≤200 ksi (1 400 MPa)100 ksi (700 MPa)for σu>200 ksi (1 400 MPa)

Cast Iron + Cast Steels:

σerb=0.45σufor σu≤600 MPa275 MPafor σu>600 MPa

Stress concentrations

- Kf:

σsc=KtS
Kt=σscS
Kf=σerbun-notchedσerbnothced
Kf=1+Kt-11+αr

- Approximations for α:

α=300σuksi1.8×10-3 in.
=300×6.89σuMPa1.8×10-3×25.4 mm

Peterson for steels (Dowling, 2013, p. 498):

logα=2.654×10-7σu2-1.309×10-3σu+0.01103

α in mm=10logα  345≤σu≤2 070 MPa
=102.654×10-7σu2-1.309×10-3σu+0.01103

Typical values are:

α=0.51 mmaluminium alloys0.25 mmannealed or normalized low-carbon steels0.064 mmquenched and tempered steels

- Kf':

Kf'-1Kf-1=fσu=q

σarb,1000'=σarb,1000Kf'
σerb'=σerbKf

Mean stress correction

| Approach | Equations |
| --- | --- |
| Modified Goodman | σar=σa1-σmσu |
| Gerber | σar=σa1-σmσu2, for σm≥0 |
| Morrow | σar=σa1-σmσf' |
| SWT | σar=σmaxσa =σm+σaσa =σmax1-R2 |
| Walker | σar=σmax1-γσaγ σmax>0 =σmax1-R2γ σmax>0 γ=-0.000200σu+0.8818(σu in MPa) |

Juvinall & Budynas (Dowling, 2013, p. Table 10.1)

Juvinall

m'=0.90kf'=kfbending, torsion (τu in σu)0.75kf'=kfaxial

Budynas:

m'=0.90σu<483 MPa0.2724x2-1.918x+4.012x=log10σu, σu≥483 MPakf'=kf

Modifying factors

σer=σerb'CsizeCloadCsurfCTCrel
σerb'=meσerbKf
σar,103=σarb,103'CloadCTCrel
σarb,103'=m'σuKf'

Size:

Csize=1.0, if d≤8 mm1.189d-0.097,if 8 mm<d≤250 mm

Load:

σer,axial=0.70σerb
Cload=0.7 for axial loading if the fatigue S-N curve was obtained from completely reversed bending loading.

Temperature:

CT=1.0 for T≤450 ℃1-5.8-3T-450, for 450<T≤550 ℃

Reliability:

## Fatigue: Large scale manufactured components

ΔσC,mod=ΔσCγMfCtCTCPWT
ΔσD=ΔσC,modNCND1m1

NR=ΔσDΔσRm1NDm1=31.5fy>ΔσR≥ΔσDΔσDΔσRm2NDm2=5ΔσD>ΔσR≥ΔσL∞ΔσR<ΔσL
NC=2×106  cycles
ND=5×106  cycles
NL=100×106  cycles

ΔσC,mod=ΔσCγMfCtCTCPWT

Partial factor for fatigue:

| Assessment | Consequence of failure |  |
| --- | --- | --- |
|  | Low | High |
| Damage tolerant | 1.0 | 1.15 |
| Safe life | 1.15 | 1.35 |

Temperature:

ΔC,HT=ΔσCEHTE20°C

0.6

0.4

0.8

Grinding & TIG dressing:

Effective stress range: Δσ=Δσ

Steel:

ΔσC=min1.3×ΔσC112

Aluminium:

ΔσC=min1.3×ΔσC45

Peening:

Effective stress range:

Δσ=ΔσR>0σmax0<R≤0.4No benefitR>0.4

Δσc,mod=Steelfy<355min(1.3Δσc, 112)Steelfy≥355min(1.6Δσc, 125)Almin(1.6Δσc, 56)

## Fracture Mechanics

Universal equation: K=βσπa

Plastic collapse:  Fpc=fyAnett

Fracture:

K=KIc
KIc=βσπaf
af=1πKIcβσ2
σf=KIcβπafr

acri=minapcfor plastic collapseaffor fracture

Stress concentration factors:

Centre cracked plate:  β=1+0.256aW-1.152aW2+12.2aW3

Single edge crack:

β=1.12-0.23aW+10.56aW2-21.74aW3+30.42aW4

Double edge crack:

β=1.12+0.43aW-4.79aW2+15.46aW3

LEFM

B, W-a, a≥2.5KIcfyt2
W≥5.0KIcfyt2

Fracture toughness estimation: KIC=11.4Cv

Lower limit: KIC=21.6Cv0.17

Note, Cv in Joule, KIC in MPa.m

Crack growth

dadN=CpΔK+mp

0NdN=aiae1CpβΔσπampda

## Pressure equipment

Pdes=P+ρgh

## Interpolation on a logarithmic scale using your ruler

log10N-log10x1log10x2-log10x1=ab
log10N=ablog10x2-log10x1+log10x1
N=10ablog10x2-log10x1+log10x1

x1

x1

N

a

b

## CONVERSIONS

1 ksi = 6.89 MPa

## Detail catgories

## Joint efficiencies

## Vessels – Dangerous gas

Figure 1:  Design categorization of vessels containing dangerous gas

## Vessels – Dangerous liquids

Source: (SANS 347, 2012)

Figure 2:  Design categorization of vessels containing dangerous liquids

## Piping – Dangerous gas

Similar graphs are available for piping of non-dangerous gas, dangerous liquids and non-dangerous liquids.

Source: (SANS 347, 2012, p. 16)

## Transportable container and vessels for dangerous gas

## Vessels: Non-dangerous gas

Source: (SANS 347, 2012, p. 12)

Figure 3:  Design categorization of vessels: non-dangerous gas